## Slide 2: Don Figer - Speaker Bio
Professor in College of Science at RIT
Professor in Astrophysical Sciences and Technology Graduate Program
Director of the Center for Detectors
Director of the Future Photon Initiative
At RIT since 2006
Previously
  Space Telescope Science Institute (operates Hubble and JWST)
  UCLA (designed optics for infrared spectrograph on Keck)
Research Interests: Detectors, Massive Stars, Massive Star Clusters, Galactic Center
3 daughters, no pets, a few plants

## Slide 3: Single Photon Detectors for NASA’s Habitable Worlds Observatory Don Figer

## Slide 4
The first Great Observatories are among the greatest missions in scientific history.
They revolutionized our understanding of the cosmos.
They were triumphs of human ingenuity.
They brought awe and wonder to our world.
They reminded us of our place in the cosmos.
They inspired a new generation of explorers.

## Slide 5
Only two remain,
and only two have been added.
By 2040, JWST and Roman will complete their missions.
A scientific golden age will end.

## Slide 6
NASA is laying the groundwork for its next flagship mission.
The Habitable Worlds Observatory will be the first telescope designed specifically to search for signs of life on planets orbiting other stars.

## Slide 7
How Will We Know We Found Life on Another Earth?

## Slide 8: Life in the Universe - Biosignatures

## Slide 9: Finding Life Outside the Solar System
The coexistence of methane (CH₄) and oxygen (O₂) in a planet’s atmosphere suggests potential alien life.
CH₄ and O₂ are highly reactive and cannot persist together without continuous replenishment.
On Earth, microbes generate CH₄ while plants and algae produce O₂, sustaining disequilibrium.
Detecting both gases elsewhere may indicate biology at work.
Spectroscopy reveals the composition of exoplanet atmospheres.
Key strategy is to look for gas combinations in disequilibrium (e.g., CH₄ + O₂, N₂O, PH₃).
Future observatories (HWO, Extremely Large Telescopes, JWST successors) will expand the search.
Typical planet signal: ~10 photons/hour/pixel → Poisson-limited regime

## Slide 10: Sensors & Detectors: A History of Discovery

## Slide 11: The Galactic Center with One Pixel (PbS)!

## Slide 12: From One Pixel to Megapixels

## Slide 13: Supermassive Black Hole – 2020 Nobel Prize

## Slide 14: Infrared Hybrid Detectors
light-sensitive material that detects infrared photons (wavelengths > ~1 µm)
silicon readout integrated circuit
detector material (e.g., HgCdTe) optimized for infrared sensitivity
“hybrid” design: infrared detector layer bonded to a silicon readout integrated circuit (ROIC) using indium bump bonds
James Webb Space Telescope prototype infrared detector on a mechanical mount affixed to a plate in a cryogenic dewar

## Slide 15: Detectors and Discovery
Charles Townes (Nobel, Laser, IR instruments)
Penzias & Wilson (Nobel, radio receiver)
Pulsars (radar)
Boyle & Smith (Nobel, CCDs)
Becklin & Neugebauer (Galactic Center in IR)
Dark Matter (image intensifiers)
Dark Energy (Nobel, CCDs)
Cosmic Microwave Background (Nobel, COBE/detectors)
Neutrinos (Nobels, PMTs)
Reinhard Genzel (Nobel, IR instruments)
James Webb Space Telescope
Hubble Space Telescope
Basically, almost every astrophysics discovery is due to new detectors and/or instrumentation.

## Slide 16: CMOS Imaging Detectors

## Slide 17: State of the Art Detector Candidates for Future NASA Missions
challenging for life finding
single-photon sensing
low dark current
near-zero read noise
multiple candidate detectors
CMOS: 9.4 Mpix
FI HWK4123
SNSPD: 0.4 Mpix (Adam McCaughan/NIST)
SPAD: Pi Imaging SPAD 5122 (Antolovic et al. 2022)
EMCCD: Teledyne e2v CCD351-00
CMOS: 163 Mpix QIS (Ma et al. 2022)
Skipper CCD: 3.5 Mpix (SENSEI Collaboration)
CMOS: Teledyne e2v CIS301/302
MKID: 20 Kpix (Mazin Lab, Breckenridge 2021)

## Slide 18: Single Photon CMOS Detector Pixel

## Slide 19: Single Photon Sensing CMOS (SPSCMOS) Detectors
low-capacitance floating diffusion sense node
high-gain response of >320 μV/e-
exceeds electronics read noise
correlated double/multiple sampling
discrete photoelectron peaks
Photon-number resolution enabled by gain > read noise
Ma, J. et al. Ultra-high-resolution quanta image sensor with reliable photon-number-resolving and high dynamic range capabilities. Sci Rep 12, 13869 (2022). https://doi.org/10.1038/s41598-022-17952-z

## Slide 20: SPSCMOS Bonding
45 nm
65 nm
Ma et al. Ultra-high-resolution quanta image sensor with reliable photon-number-resolving and high dynamic range capabilities. Sci Rep 12, 13869 (2022).

## Slide 21: SPSCMOS Image Sensors
QIS CMOS
1 Megapixel Sensors
1.1 μm pixels
HWK4123
9.4 Megapixel
4.6 μm pixels
ORCA-QUEST
HWK4123

## Slide 22: Characterize Detectors

## Slide 23: Detector Characterization Table

## Slide 24: Photon Counting Under Changing Illumination

## Slide 25: Dark Current

## Slide 26: Read Noise

## Slide 27: Quantum Efficiency

## Slide 28: Measure and Mitigate Radiation Effects on Detectors

## Slide 29: Radiation Test Program
 | SEE/SEU (L2 & JEO) | DDD (L2 & JEO) | TID (L2) | TID (JEO)
facility | MSU Facility for Rare Isotope Beams | UC Davis Crocker Nuclear Laboratory |  | RPI Gaerttner Linear Accelerator (LINAC) Center
mission equivalent | ten 11-year missions at L2 |  |  | 5.5 year mission at JEO
total exposure | See LET Curve | 1e9 MeV g(Si)-1 | up to 50 krad | >1 Mrad
beam pulse/exposure | one per LET | multiple cumulative exposures |  | multiple cumulative exposures
particle(s) | Ne, Ar, Co, Kr, Ag, Xe, Tm, Au | protons |  | electrons
energy | see ion cocktail | 60 MeV |  | 15 - 25 MeV
measurement | changes in pixel signal, detector bias and power, and 1d greyscale pattern |  |  | 
total fluence | 1e7 ions/cm2 or 100 events | >3e11 p/cm2 |  | >1e14 e-/cm2
light level | dark | dark |  | dark
cooling | no cooling | active cooling |  | active cooling
environment | in-air | vacuum |  | vacuum
Detector | SEE | DDD/TID (krad) | TID (Mrad)
 | Heavy Ions | Protons | Electrons
QISSAT1-2 |  | ✓ | 
HWK4123_1427 | - | - | -
HWK4123_1430 | - | - | 
HWK4123_1438 | - |  | 
HWK4123_1441 |  |  | 
HWK4123_1442 |  |  | 
HWK4123_1447 |  | - | 
HWK4123_1450 |  |  | 
HWK4123_1453 |  |  | 
HWK4123_1475 |  |  | -
HWK4123_1479 |  |  | -

## Slide 30: Characteristic Effects
trap-assisted leakage
  bulk traps capture electrons
  trap states enable recombination paths into the substrate
  changes RTN frequency and increases 1/f noise
surface / interface damage
  oxide charge and interface traps near TG / FD / SF / RST alter local potentials
  can shifts reset-transistor threshold voltage
reset-transistor / barrier-region damage
  threshold-voltage shifts changes reset effectiveness
  gate-oxide damage increases reset leakage
  produces apparent FD-reset drift after reset
parasitic conduction and edge inversion
  positive oxide charge buildup along shallow-trench isolation (STI) edges forms weak conductive channels
  provides paths to leak electrons leading to FD-reset drift
  may couple to or perturb neighboring pixels
STI

## Slide 31: Develop Single-Photon Sensing NIR Photodiode

## Slide 32: Design a Single-Photon Sensing NIR Photodiode
developed InGaAs and Si TCAD model of photodiode using Synopsys Sentaurus
evaluating photodiode performance with several 2D and 3D designs
migrating structure to MCT to compare to Si and InGaAs predecessor

## Slide 33: Evaluate Detectors with On-Sky Observations
Notes: Red images: infrared detector testing
Galaxy: NGC7331 with supernova (July 2025) near galactic center

## Slide 34: Univesrity of Rochester’s C.E.K. Mees Observatory
Naples, NY

## Slide 35: Telescope Observing with SPSCMOS Detectors
measuring detector non-linearity using star clusters and comparing to results from lab experiments
measuring quantum efficiency using the expected and measured counts for stars
comparing photometric results to literature
Johnson - BVR
H-Alpha
Notes: Star field: M36
Nebula: Bubble Nebula

## Slide 36: M36 Delta-magnitude Diagram – Edwin Alexani
compare photometric results to literature
reject photometry with magnitude error beyond ±0.5
calibrate and correct non-linearity from photometry data
compare non-linearity from photometry to lab experiments (~10 – 20 % at low flux)
measure scatter of photometry (~0.04 mag for magphot = 14 and brighter)
investigate asymmetry at low flux
Notes: The plot shows photometry data for M36. Each color = photometric band, as labeled in the legend.
The y-axis = apparent magnitude of stars (relative photometry), x-axis = difference from our photometry to catalog query
Reject any delmag outside +/- 0.5
Then data is corrected for non-linearity using the photometry data (not the lab data), and we can then to compare to lab results
The shift from correcting the data is 10-20% for low flux which is similar to the lab results
For mag 14 and above, the STDDEV is ~0.04 mag
Below mag 14, the scatter is larger, ~0.2, and is attributed mainly to low SNR and a few contamination by nearby stars

## Slide 37: Develop Roadmap for Space-based SPSCMOS Detectors

## Slide 38: Roadmap for Space-based SPSCMOS Detectors
reduce dark current to <10-4 e-/s/pix
improve quantum efficiency at shorter wavelengths (50%) with backside engineering
improve quantum efficiency at longer wavelengths (20% at 1 mm) with thicker pixels
mitigate charge loss/trapped charged during transfer which cause nonlinearity at low signal
prevent freeze-out due to black sun effect at low temperatures (<185 K)
implement correlated multiple sampling
remove restriction on number of pulses per signal in wavetable

## Slide 39: Nonlinearity
QUEST Gen 2 result (Layden 2026)
QUEST Gen 1 preliminary result
Notes: Layden 2026 : bottom panel of Figure 4 a
Our result: QUEST experiment that was stitched, which is the cause of the two breaks near 100ms

## Slide 40: Nonlinearity
QUEST Gen 2 result (Layden 2026)
QUEST Gen 1 preliminary result
Notes: Layden 2026 : bottom panel of Figure 4 a
Our result: QUEST experiment that was stitched, which is the cause of the two breaks near 100ms

## Slide 41: Nonlinearity
QUEST Gen 2 result (Layden 2026)
HWK4123-1450 preliminary result
Notes: Layden 2026 : bottom panel of Figure 4 a
Our result: QUEST experiment that was stitched, which is the cause of the two breaks near 100ms

## Slide 42: Nonlinearity
QUEST Gen 2 result (Layden 2026)
HWK4123-1450 preliminary result
Notes: Layden 2026 : bottom panel of Figure 4 a
Our result: QUEST experiment that was stitched, which is the cause of the two breaks near 100ms

## Slide 43: Black Sun Effect and Freeze-out
Black sun effect triggers in some sections of the HWK4123 at low enough temperature
This prevents testing at lower temperatures for the full sensor

## Slide 44: Single Photon Counting Spectrograph – Edwin Alexani
combine single photon counting detector with photonic spectrograph
reduce SWaP
detect biosignatures in exoplanets
simulate performance and compare to HWO simulator
design prototype in visible range (500-800nm)

## Slide 45: Summary
challenging science
observe low photon flux sources
detect biosignatures on exoplanets
develop detector technologies for HWO single-photon sensing in UV, optical, and NIR
Recent Publications:
Gallagher, J. P., Buntic, L., Deng, W., Fossum, E. R., and Figer, D. F. 2024, Radiation tolerance of a single-photon counting complementary metal-oxide semiconductor image sensor, J. Astron. Telesc. Instrum. Syst. 10(3), 036003, doi: 10.1117/1.JATIS.10.3.036003.
Gallagher, J. P., Buntic, L., Alexani, E., Bouthsarath, K., and Figer, D. F. 2024, Characterizing radiation-tolerant single photon resolving CMOS detectors, Proceedings Volume 13103, X-Ray, Optical, and Infrared Detectors for Astronomy XI; 131030S, Yokohama, Japan, https://doi.org/10.1117/12.3019105.
Gallagher, J. P., Buntic, L., Figer, D. F., Deng, W. 2024, Characterization of single-photon sensing and photon-number resolving CMOS image sensors, Proc. SPIE 12191, X-Ray, Optical, and Infrared Detectors for Astronomy X, Montreal, Canada, https://doi.org/10.1117/12.2629006

## Slide 46: Recent Publications
Recent Publications:
Hoon, N., Alexani, E., and Figer, D. F. Opto-Mechanical Design and Analysis of a Compact Photonic Spectrograph for Space Application,M.S. Thesis, 2025.
Alexani, E., Gallagher, J. P., and Figer, D. F. Single-Photon CMOS Detectors for HWO,proceedings of Towards the Habitable Worlds Observatory: Visionary Science and Transformational Technology, Washington, DC, 28–31 July 2025.
Alexani, E., Gallagher, J. P., Wolcott, M., and Figer, D. F. Single-Photon CMOS Detectors for HWO,proceedings of Towards the Habitable Worlds Observatory: Visionary Science and Transformational Technology (Poster), Washington, DC, 28–31 July 2025.
Figer, D. F. Sensors and Detectors for Physical and Chemical Sciences – Finding Aliens,CHIPS for Science Conference (Invited Talk), Austin, TX, 29–30 October 2025.
Gallagher, J. P., Buntic, L., Alexani, E., Bouthsarath, K., and Figer, D. F. Characterizing radiation-tolerant single photon resolving CMOS detectors, Proceedings Volume 13103, X-Ray, Optical, and Infrared Detectors for Astronomy XI; 131030S, Yokohama, Japan, 2024.

## Slide 47: Team Members

## Slide 48: Arches Cluster - JWST Cycle 4

## Slide 49: Future Photon Initiative Center for Detectors

## Slide 50: Future Photon Initiative
Future Photon Initiative: develops photonic devices in pursuit of answers to grand questions, leveraging efforts of existing RIT research groups using the generation, transmission, manipulation, absorption, and detection of
solar energy, biophotonics, high performance imaging, astrophysics, quantum, and communication.
Eight groups: Center for Detectors, Integrated Photonics Group, Nanolithography Research Lab, NanoPower Research Labs, Photonic Systems Lab, Photonics and Optics Workforce Education Research, Semiconductor Nanofabrication Lab, and the Simone Center for Innovation and Entrepreneurship.
43 ongoing grants with $7.7M funding

## Slide 51: Center for Detectors

## Slide 52: Questions

## Slide 53: Backup Slides

## Slide 54: Integrated Photonics Group

## Slide 55: First Astronomical CCD Image

## Slide 56: RIT CHIPs-related Activities

## Slide 57: RIT CHIPS-Related Programs
NSF ExLENT: EMERGE-MICRO
Sponsor: NSF TIP & EDU Funding: ~$1M | 2024 – 2027
Develop a pilot pipeline for community college students through A.S. → B.S. in Microelectronic Engineering.
Hands-on cleanroom training, co-op placements, and industry-guided research.
Collaborators: MCC, FLCC, GlobalFoundries, Micron, University of Rochester evaluator.
NSF NRT: CMOS+X Graduate Training
Sponsor: NSF NRT Funding: ~$3M | 2024 – 2029
Provide graduate (M.S. & Ph.D.) fellowships (~20 doctoral) in interdisciplinary semiconductor research.
Focus areas: CMOS + AI, biomedical, optoelectronic, photonic, nanoelectronics, quantum, packaging.
Goal: Train 170+ next-gen engineers & scientists, emphasizing technical and professional development components.
NSF: UPWARDS for the Future
Sponsor: NSF | (UW lead) Funding: ~$10M | 2023 – 2028
U.S.–Japan university partnership engaging six U.S. and five Japanese universities.
Activities: Student exchanges, faculty visiting programs, certification, curriculum development, focused semiconductor and memory-centric research.
Objective: Build a globally connected, skilled microelectronics workforce aligned with industry needs.
DoC: BRIDGE for Microelectronics
Sponsor: Dept of Commerce/NIST CHIPS Act Funding: ~$1.5M | 2025 – 2027
Build graduate education program to train 555 students across bachelor’s, master’s, and certificate tracks in microelectronics.
Includes new online certificate offerings, industry collaboration, and student support.
Part of NSTC Workforce Partner Alliance under CHIPS Act, scaling semiconductor workforce ecosystem.
Industry Partners: Micron, GlobalFoundries, Northrop Grumman

## Slide 58: RIT-CHIPS News
This list includes NSF public records and RIT/local news releases about our CHIPS-related workforce efforts here:
NSF ExLENT:
  https://nsf.elsevierpure.com/en/projects/beginnings-empowering-minds-through-experiential-learning-researc
  https://www.rit.edu/news/rit-expands-its-workforce-initiatives-semiconductor-industry
NSF NRT:
  https://www.nsf.gov/awardsearch/showAward?AWD_ID=2345983&HistoricalAwards=false
  https://www.rit.edu/news/nsf-awards-rit-nearly-3-million-advance-semiconductor-technologies
NSF UPWARDS for the Future:
  https://nsf.elsevierpure.com/en/projects/us-japan-university-partnership-for-workforce-advancement-and-res
  https://www.rochesterfirst.com/development/inside-upwards-at-rit-an-international-semiconductor-education-exchange-program/
Department of Commerce BRIDGE for Microelectronics Program:
  https://www.nist.gov/chips/rochester-institute-technology-rit-rochester
  https://www.nist.gov/news-events/news/2024/09/biden-harris-administration-launches-nstc-workforce-center-excellence
  https://www.rochesterfirst.com/news/local-news/rit-awarded-1-5-million-to-train-555-students-in-semiconductor-program/
You can find a full list of RIT CHIPS news here: https://www.rit.edu/news/semiconductor-chips

## Slide 59: Sensors and Detectors All Around Us
Everyday applications
  phones
  cars
  defense
  medicine
Cutting edge applications
  high energy physics
  astrophysics
  quantum information science and technology
Semiconductors as enablers

## Slide 60: CMOS Imaging Detectors in Astrophysics
CMOS imaging detectors transformative for Astrophysics
HST, JWST, Rubin, Roman, HWO
United States world leader in CMOS imaging detectors, although threats are constant

## Slide 61: Infrared Hybrid Array
light-sensitive material that detects infrared photons (wavelengths > ~1 µm)
silicon readout integrated circuit
detector material (e.g., HgCdTe) optimized for infrared sensitivity
“hybrid” design: infrared detector layer bonded to a silicon readout integrated circuit (ROIC) using indium bump bonds

## Slide 62: Alien Life
The coexistence of methane (CH₄) and oxygen (O₂) in a planet’s atmosphere suggests potential alien life.
CH₄ and O₂ are highly reactive and cannot persist together without continuous replenishment.
On Earth, microbes generate CH₄ while plants and algae produce O₂, sustaining disequilibrium.
Detecting both gases elsewhere may indicate biology at work.

## Slide 63: Beyond CH₄ + O₂
Additional chemical reactions may hint at life or habitability:
  CO₂ + H₂ → CH₄ (geological or biological)
  N₂ + O₂ imbalance (linked to biological cycling)
  Trace gases like NH₃ or PH₃ that require active replenishment.
These broaden the search beyond methane and oxygen alone.

## Slide 64: Life and CH4 + O2 Reaction

## Slide 65: Very Low Light Level - ExoPlanet Imaging
The exposure time required to achieve SNR=1 is dramatically reduced for a zero read noise detector, as compared to detectors with state of the art read noise.
Notes: The table gives exposures times to produce SNR=1 for a typical planet detection space mission. Note the dramatic reduction in time required for a zero noise detector. R=100 is assumed, and the effective planet flux is about 10 photons/hour per pixel. The nearby starlight is suppressed at the 10^-10 level by optical nulling. Zodiacal light contributes about 0.0015 electrons/s/pixel.

## Slide 66: Signal-to-noise Ratio (SNR)
discoveries
better detector, higher SNR
In some cases, SNR is dominated by the source itself.
Longer integrations increase SNR!

## Slide 67: 3.2 Gigapixel Focal Plane in LSST
Large Synoptic Survey Telescope 3.2 Gpixel focal plane with 220 CCDs
4-side buttable, highly integrated focal plane rafts
future technologies and enhanced capabilities

## Slide 68: Applications for SPSCMOS
use on future flagship missions like HWO
use in high radiation environment missions (i.e. Europa Clipper, Parker Probe)
observe faint rapid transient events
integrate with photonic technology for spectroscopy
observe Earth at nighttime