## Slide 1: DETECTORS AND ADVANCED COATINGS FOR EFFICIENT UV/OPTICAL/NIR SYSTEMS
Shouleh Nikzad
M. E. Hoenk, A. Carver, T.J. Jones, J. Hennessy, A. Jewell, E. Hamden, &T. Goodsall
Jet Propulsion Laboratory, California Institute of Technology
National Aeronautics and Space Administration
© 2013 California Institute of Technology. Government sponsorship acknowledged.
Scientific Detector Workshop
Florence, Italy
7 October 2013
Notes: 1

## Slide 2
Bob Beach
Paul Maker
Todd Jones
Doug Bell
Todd Veach
Alex Carver, ECH
Matt Dickie
Nicole Lingner, Grad Caltech
John Hennessy
Caltech Postdoc
scholar
Sam Cheng, Grad, USC
Alex Miller, Grad
ASU
Tim Goodsall, ECH
Erika Hamden
NESSF, Columbia
Michael Hoenk
Frank Greer
April Jewell, NPP fellow
Todd Veach, PhD
Grad, ASU
Doug Bell

## Slide 3
Dark Matter
Future UV/Optical/NIR Missions
Contrast Imaging: Dark matter/Dark Energy
JDEM/SNAP
Protoplanetary disks to exoplanets
Star Formation
Mapping IGM

## Slide 4
High Performance UV/Vis/NIR Si Detectors with Atomic-scale surface/interface engineering
  Delta doping plus ALD AR coatings
  Enables high efficiency, stable response, and reliable performance
Large-Scale Processing for High Throughput & High Yield
  Wafer level processing (up to 8-inch wafers), batch processing
  Wafer scale devices (taking up the entire 8-inch wafer area)
Examples of Science Motivations and Device Solutions/Deliveries
FUV EMCCD (FIREBall)
  UV P-channel CCDs (CHESS)
  Broadband (WaSP)
Brief Note on work on Reflective Optical Coatings
Outline
See Poster by Hoenk et al, Superlattice-doped detectors

## Slide 5: High Performance Silicon Imaging through Back-illumination
Key detector performance parameters depend on back illumination for all silicon imaging devices.
These key parameters include wide spectral range, efficiency, resolution, stability of response, dark current, and high fill factor

## Slide 6
Delta doping for surface
bandstructure engineering
and passivation
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-

## Slide 7: 100% Internal QE with Delta doping through Atomically Precise Interface Engineering
100% internal quantum efficiency, uniform, and stable (QY has been removed so maximum QE is 100%).
Extreme UV measurements were made at SSRL
Compatible with AR and filter coating: response can be tailored for different regions of the spectrum

## Slide 8
Al
CH3
CH3
CH3
wafer
OH
OH
Al
CH3
CH3
CH3
Silicon wafer
O
O
Al
CH3
CH3
Al
CH3
CH3
CH4
CH4
Silicon wafer
O
O
Al
CH3
CH3
Al
CH3
CH3
Silicon wafer
O
O
Al
Al
O
O
O
C
O
O
OH
OH
Silicon wafer
O
O
Al
Al
O
OH
OH
Precursor Dose
Precursor Purge
Plasma/Reactant Dose
Reactant Purge
Initial Surface
Cycle Repeats to Grow Additional Monolayers
High External QE with Atomic Layer Deposition through Atomically Precise Interface Engineering
What is ALD?
Surface reaction mediated deposition
ALD cycles are repeated until desired film thickness is achieved
Metals, Nitrides, and Oxides are achieved through choice of precursor and reactant species
Can achieve thin film deposition or surface modifications at near room temperature
Results in smooth, stoichiometric, thin layers.
Abrupt interfaces and precision control makes ALD perfectly suitable for multilayer coatings
Number of Cycles
Thickness
Plasma

## Slide 9: High Precision AR Coatings
Reflectance (%)
Wavelength (nm)
Model – SiO2/HfO2/Al2O3/Si
Actual – SiO2/HfO2/Al2O3/Si
Si Baseline Reflectance
Incorporating diffusion barriers into the design, when appropriate, allows us to deposit films with behavior predicted by our model.
Multilayers are feasible with these device integrated coatings. Opens the door for other types of coatings (e.g. visible blind coating, interference filters, etc.) deposited by ALD.
Reproducibility and accuracy of the ALD technique enables rational design and fabrication of AR coatings at the nanometer scale.
Wavelength dependence of coating performance correctly predicted by AR coating models based on precision UV ellipsometry measurements

## Slide 10
Molecular Beam Epitaxy (MBE) and Atomic Layer Deposition (ALD) uniquely enable atomic-level engineering of surfaces/interfaces to achieve high efficiency, stable response, and low dark current in back-illuminated silicon arrays.
This is true for UV/Visible/NIR and especially true in UV where absorption happens within nanometers of the surface
Versatile techniques applicable to essentially all silicon detectors and imagers
MBE Delta doping and ALD-AR coatings resulting in
High Performance Silicon Imagers

## Slide 11
Delta doped EMCCD
Higher QE, lower noise
up to 10x S/N
MCP Data (GALEX)
Higher QE CCD with gain
Normal CCD
EMCCD Simulation has 4x S/N of GALEX
P. Morrissey, KISS Workshop on Next Gen UV Instrument Technologies, August 2011

## Slide 12: Electron Multiplied CCD (EMCCD)
Charge multiplication
register
EMCCD (Electron Multiplied CCD) operates by adding avalanche gain in the final register (gain or multiplication register). Combined with low noise readout this can translate into single photon counting.
P. Pool e2v
If1
If2
If3
Regular CCD
Charge Transfer
Charge transfer

## Slide 13: Delta doped EMCCD
0.5
0.5Kx1k, 13 µm EMCCD
Quantum Efficiency of Delta doped EMCCD
Delta doped Electron Multiplied CCD (EMCCD) for solid state photon counting spectroscopy

## Slide 14: > 50% Quantum Efficiency Achieved in UV
Achieved by Atomic Control at the surfaces and interfaces with Delta-doping and ALD Antireflection Coating
Delta doping & Atomic Layer Deposition o f standard CCDs & EMCCDs
Nikzad, et al. Applied Optics, 2012

## Slide 15: Wafer-Scale Processes

## Slide 16
First results
High throughput, high yield processing of high performance detectors
Delta doping up to 8-inch diameter wafers
Batch processing multiple wafers
8-inch Wafer Silicon Molecular Beam Epitaxy (MBE)

## Slide 17
e2v CCD97 wafer
Process steps…
Wafer-wafer bonding
Thinning
MBE growth
ALD coating
Patterning
Etching
Dicing
Packaging
Wafer-scale process flow
E2v CCD97 wafer: after bond pad exposure
Wafer with CMOS imaging arrays in 8-inch MBE
Superlattice-doped Electron Multiplying CCD
Handle wafer (~800 µm)
EMCCD electronics
EMCCD silicon (~10 µm)
MBE-doped Si
ALD oxide
Veeco 8-inch Silicon MBE at JPL’s Microdevices Lab

## Slide 18
Six R-grade e2v CCD97’s from the bonded, thinned, delta-doped wafer 18 have been packaged, wire-bonded and are being tested. One is AR coated with the FIREBALL multilayer design

## Slide 19: FIREBall-2
An EMCCD wafer (p-type substrate) was cored down to 4 inches, bonded, thinned, and sections of it were diced into die that were delta doped. Above are the photograph of the device and the preliminary measurements showing high QE in the UV indicating successful delta doping.
Funded balloon under ROSES-APRA
PI: Chris Martin
Detector range: 195-205 nm, 200 nm center require QE > 50%
FIREBall-1 flew a GALEX spare detector which was an MCP.
Collaboration also with David Schiminovich, Erika Hamden, Columbia U
Alice Reinheimer, Peter Pool, P. Fochi, et al e2v

## Slide 20: Preliminary QE Results on AR Coated (5-Layer), Delta Doped EMCCD (0.5 Megapixel, CCD97)
5-layer, delta doped CCD97
Location of the peak matches the model!
More measurements required to obtain absolute QE

## Slide 21
Delta (& super-lattice) doping 12 Megapixel LBNL Fully Deplted CCDs
Wafer Probe at -65°C
Four 12-Megapixel, 10.5 µm pixel, p-channel CCD
Processed by N-type delta doping
63% Yield for Science grade CCD measured by LBNL
Collaborations with Chris Bebek and Steve Holland, et al. at LBNL
See S. Holland talk

## Slide 22
Chart: 127299.21.2 Superlattice-Doped CCD Preliminary QE - PD Mode Vsub=50 V, -140 C
| 300 | 320 | 340 | 360 | 380 | 400 | 420 | 440 | 460 | 480 | 500 | 520 | 540 | 560 | 580 | 600 | 620 | 640 | 660 | 680 | 700 | 720 | 740 | 760 | 780 | 800 | 820 | 840 | 860 | 880 | 900 | 920 | 940 | 960 | 980 | 1000 | 1020 | 1040 | 1060 | 1080 | 1100
Distance Cal. QE_Pass1 | 24.2244 | 26.0092 | 27.3116 | 26.6018 | 34.7369 | 43.3196 | 47.9518 | 51.1622 | 53.1185 | 54.8586 | 56.6772 | 57.8929 | 58.8137 | 59.5504 | 60.5836 | 60.9305 | 61.6168 | 62.471 | 62.6259 | 63.1439 | 63.5218 | 64.6341 | 65.4182 | 65.9657 | 66.6078 | 66.7036 | 67.1957 | 67.9444 | 68.3427 | 68.8611 | 68.4588 | 66.3189 | 62.4245 | 55.8989 | 45.7152 | 32.3419 | 17.0472 | 6.1424 | 2.9014 | 1.3654 | 0.76923
Distance Cal. QE_Pass2 | 25.7198 | 26.9899 | 27.1349 | 28.7941 | 40.0971 | 45.8107 | 49.6468 | 52.2024 | 54.037 | 55.7921 | 57.3207 | 58.3734 | 59.1982 | 60.0874 | 60.7575 | 61.3008 | 62.071 | 62.5511 | 62.8567 | 63.3035 | 64.0647 | 65.0375 | 65.7149 | 66.2995 | 66.6626 | 66.9024 | 67.5556 | 68.1318 | 68.6663 | 68.8124 | 67.6139 | 64.6845 | 59.5624 | 51.1588 | 39.1732 | 24.2803 | 9.5299 | 4.1803 | 2.0379 | 0.9329 | 0.45148
QE_25C_Pass1 | 23.5154 | 29.0494 | 31.6994 | 32.0546 | 35.3829 | 44.0599 | 48.4406 | 51.3345 | 53.025 | 54.5645 | 56.1696 | 57.2037 | 57.9627 | 58.5524 | 59.4582 | 59.6794 | 60.2311 | 60.942 | 60.9888 | 61.341 | 61.5351 | 62.4333 | 63.079 | 63.5133 | 64.0399 | 63.9714 | 64.2049 | 64.6264 | 64.7825 | 65.2664 | 65.6233 | 65.5734 | 65.4915 | 64.6396 | 61.7264 | 57.1463 | 49.4327 | 39.0503 | 26.7419 | 18.2819 | 12.3788
QE_25C_Pass2 | 30.0213 | 31.9821 | 32.4469 | 32.9756 | 41.332 | 46.7372 | 50.215 | 52.3851 | 53.9018 | 55.3652 | 56.6457 | 57.487 | 58.1344 | 58.8692 | 59.3986 | 59.8279 | 60.4585 | 60.8394 | 61.0188 | 61.3171 | 61.9179 | 62.729 | 63.3184 | 63.7885 | 64.0357 | 64.0998 | 64.4263 | 64.7205 | 65.0575 | 65.5046 | 65.6603 | 65.6232 | 65.2643 | 63.3295 | 59.4618 | 53.2797 | 44.1967 | 32.9154 | 22.597 | 15.418 | 10.191
25 C
-140 C

## Slide 23: Characterization in FUV, UV, and Visible

## Slide 24: Far UV Rocket
CHESS (sounding rocket, PI:Kevin France CU)
Collaboration with Paul Scowen, Todd Veach*, Alex Miller, ASU
FUV, 3.5kx3.5k (100 – 160 nm) bare, delta doped delivered to CHESS

## Slide 25: Far UV Rocket
CHESS (sounding rocket, PI:Kevin France CU)
Collaboration with Paul Scowen, Todd Veach*, Alex Miller, ASU
FUV, 3.5kx3.5k (100 – 160 nm) bare, delta doped delivered to CHESS
3-4x QE gain over MCP

## Slide 26
Delta doping Large Area Array at Wafer Level
STA 2kx2k CCDs (n-channel, p-type delta doping)

## Slide 27
Photographs of an STA 3600 imager diced from a delta doped 200 micron wafer. It has been flattened against AlN and mounted in a AlN frame prior to wire bonding to flex.
New packagaing to accommodate WaSP requirements are under development
Delta-doped, AR coated fully depleted 2kx2k STA devices for WaSP guide and focus CCDs
(320 – 1000 nm)
WaSP for Palomar
WaSP

## Slide 28
Chart: Optical Performance of ALD Grown AR Coatings

## Slide 29: ALD Coatings for Broadband Response

## Slide 30: Breakthrough Results in Deep UV with Alacron/Fastvision
PI: Michael Hoenk. “Superlattice-doped”, new design, Hoenk (US patent)
3 Mpxl CMOS, low noise, 150 frames/ second, 8” wafers.
Demonstrated unprecedented stability. 500x saturation exposure to Excimer laser (100 million high energy pulses of the laser hitting the device!!).
Called a breakthrough by industry!!
See Michael Hoenk’s poster

## Slide 31: Reflective Coatings for Astrophysics & Planetary Applications
Purple: neutral gas (trace species)
Blue: neutral gas (dominant ion)
Green: warm, (intermediate ionization) plasma
Red: highly ionized plasma
Reflective coatings determine the mission architecture for any UV mission (FUSE, HST/COS, etc.)
FUV has a significant number of spectral lines that are of great interest to astronomers
Far Ultraviolet Spectroscopic Explorer (FUSE)
Credit: T.A. Rector and B.A. Wolpa, NOAO, AURA, and NSF.
Collaboration with: Kevin France
CU - CASA
PI: W. Moos
Johns Hopkins
Notes: This is a false-color image of the star AE Aurigae (bright source of light slightly off center of image) embedded in a region of space containing smoke-like filaments of carbon-rich dust grains, a common phenomenon. Such dust might be hiding deuterium, an isotope of hydrogen, and stymieing astronomers' efforts to study star and galaxy formation. The FUSE satellite has surveyed the local deuterium concentration in the galaxy and found far more than expected. Because deuterium is a tracer of star and galaxy evolution, this discovery could radically alter theories about how stars and galaxy form.

## Slide 32: Benefits of Improved Mirror Coatings
 | Size
FUSE | ~6 m
FUSE w/ improved coatings | ~3 m
Aluminum mirrors require protective coatings (i.e. LiF or thick MgF2) to prevent oxidation which would otherwise destroy reflectivity in the FUV
Coatings also important in optical wavelengths as they affect polarization
By using very thin, but high quality, MgF2, both issues can be addressed simultaneously.
  Very thin coatings minimize impact on polarization of incident light
  Thin films of MgF2 (1-2 nm) enable higher reflectivity (due to lower absorption losses) than LiF or thick MgF2
Reflectivity (%)
Wavelength (Å)
MgF2 (1 nm)
MgF2 (2 nm)
MgF2 (HST)
LiF/Al (FUSE)
Modeled using TFCalc Software
Collaboration with K. France, M. Beasley* (CU) F. Greer* ( JPL)

## Slide 33: ALD Chemistry for MgF2
Chart: Temperature Dependence of MgF2 Deposition
| 250 | 200 | 150
Index | 1.42 | 1.42 | 1.42
GPC | 1.3333 | 1.2867 | 1.3867
Chart: HF Purge Time
| 7 | 15 | 20 | 25 | 30 | 20 | 27 | 26
GPC (A/cycle) | 8.2267 | 3.18 | 2.2667 | 1.24 | 1.4267 | 2.0933 | 1.6467 | 1.7733
Robust and Facile Chemistry
This reaction occurs readily. The Mg precursor has a high vapor pressure, is easy to work with, and can be used for other reactions (i.e., MgO).
5Mg(tmhd)2(g) + 2TaF5 (g) ---> 5MgF2(s) + 2Ta(tmhd)5(g)
Published Process*
Challenging Chemistry
Mg precursor has very low vapor pressure. Ta precursor will react with any oxygen in the system leading to Ta2O5 rather than MgF2.
*Pilvi, T.; et al., Chem. Mater., 20 (2008) 5023.
Mg(EtCp)2(g) + 2HF (g) ---> MgF2(s) + 2H(EtCp)(g)
JPL Developed Process♩
♩Greer, F.; et al., in preparation
Notes: Bis(2,2,6,6-tetramethyl-3,5-heptanedionato) magnesium
Bis(ethylcyclopentadienyl) magnesium

## Slide 34: Characterization
ALD Al-coated substrate
Bare substrate
ALD Aluminum
ALD MgF2 on Aluminum
E-Beam Evaporated Aluminum

## Slide 35: Opportunity to fly on SLICE*
Mirror from SLICE will become available for coating soon. Future flights with ALD coatings
*U of Colorado rocket: Sub-orbital Local Interstellar Cloud Experiment (SLICE)
PI: Kevin France

## Slide 36: Summary
  Atomic scale surface engineering through MBE and ALD enable high efficiency, stable response in detectors
  Wafer scale and batch detector processing enable high throughput, high yield compatible with mission delivery time scale and cost
Delivery to FIREBall, CHESS, WaSP Progress
  Optical coatings also using ALD allows high efficiency reflective coatings for more efficient systems.

## Slide 37: Thank you for Your Attention!

## Slide 38: CCD201, bonded and thinned

## Slide 39: ALD AR coatings, using CCD97
CCD97, bonded, thinned, delta doped
Shadow mask

## Slide 40: AR coatings, using CCD97

## Slide 41
Human-Eye-inspired curved arrays
Enabling the very compact & the very large cameras
flat
Curved
Flat

## Slide 42
Camera for Laboratory Characterization
and
for on-sky observation
And

## Slide 43: Why does the peak shift?

## Slide 44
Bandstructure engineering for optimum device performance with atomic layer control over silicon surface
Delta doping technology
Low temperature process, compatible with VLSI, fully -fabricated devices (CCDs, CMOS, PIN arrays)
0.004 µm
Delta-doped layer
(boron in single atomic layer)
Native oxide
0.002 µm
original Si
~ 15 µm
CCD
frontside
circuitry
Thinned CCD
Hoenk et al., Applied Physics Letters, 61: 1084 (1992)

## Slide 45
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-

## Slide 46
QE > 80% with ALD Multilayer Coatings
Ref: Erika T. Hamden, et al, Paper 8453-8 of Conference 8453
1 Megapixel prototype with Cassini CCD
Hamden et al., SPIE, Astronomical Instrument and Telescopes, Amsterdam, July 2012
Response (from reflectivity and absorption) measured on blank silicon and fused silica wafers and on conventional CCDs looks good but the position of the peak is shifted

## Slide 47: Performance of ALD Protected Mirror
Measured reflectance of 20 nm of ALD MgF2 protected aluminum is as good as COTS mirror (perhaps better)
  Approaches theoretical performance of protected aluminum
Need to extend these measurements to the FUV and to thinner ALD MgF2 films
Greer, F.; et al., in preparation
Reflectivity (%)
Compared to Bare Al Reference Mirror
Wavelength (nm)
Bare E-beam Al
E-beam Al with MgF2 coating
Bare E-beam Al (w/XeF2 treatment)
E-beam Al (XeF2 treatment)
with MgF2 coating

## Slide 48: XPS Characterization of ALD MgF2
ALD MgF2 [Mg(EtCp)2 + HF] yields similar film stoichiometry to a thermally evaporated film, but with higher resistance to oxidation after air exposure.
Evaporated MgF2
ALD MgF2
Binding Energy (eV)
Binding Energy (eV)
Greer, F.; et al., in preparation
Greer, F.; et al., in preparation

## Slide 49: ALD MgF2 - Performance
Took simplified approach to mirror coating problem initially to look at just the performance of ALD MgF2 itself
  No complications of ALD Al nucleation and cross-contamination of the films in same chamber
  Used glass substrate with e-beam evaporated aluminum
ALD MgF2 is amorphous as deposited at 250oC.
  Surprising, but extremely good result for application as protective layer
TEM Prep Layers
TEM Prep Layers
ALD MgF2
ALD MgF2
Evaporated Aluminum
Evaporated Aluminum
Greer, F.; et al., in preparation

## Slide 50
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
Trapping of photo-generated charge

## Slide 51
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
Trapping of photo-generated charge
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-

## Slide 52
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-