## Slide 1: Performance Improvements for Fully Depleted Charge-Coupled Devices
S.E. Holland, C.J. Bebek, J.H. Emes, D.E. Groom, S. Haque, A. Karcher,
W.F. Kolbe, J.S. Lee, N.P. Palaio, C.H. Tran, and G. Wang
Lawrence Berkeley National Laboratory
F. Dion, R. Frost, and R. Groulx
Teledyne DALSA Semiconductor

## Slide 2: Introduction
Major results since 2009 SDW
  CCDs for the Dark Energy Survey Camera and BOSS
DECam – 62 2k x 4k’s and 12 2k x 2k’s (15µm pixels)
  1st light September 2012
BOSS – 2 4k x 4k’s (15 µm pixels)
  In operation since 2009 with > 2 million spectra taken
  250 µm thick CCDs

## Slide 3: Introduction
Major results since 2009 SDW (cont’)
  R&D efforts to improve noise, readout speed and QE
Internal LBNL R&D funding
Wafer delivery Fall 2010
  6 and 12 channel CCDs (10.5 µm pixels)
  Low noise amplifiers (buried contacts)
  Skipper CCD (sub-electron noise)
  Fast CCDs for direct x-ray detection
    196 amplifiers
Department of Energy NNSA grant
Wafer delivery late 2012
  16 channel CCDs (10.5 µm pixels)
    4k x 4k and 4k x 2k
  Low noise amplifiers (buried contacts)
    Not successful this run

## Slide 4: Introduction
Major results since 2009 SDW (cont’)
  R&D efforts to improve noise, readout speed and QE
Internal LBNL R&D funding (FY 2013)
Wafer delivery October 2013
  4k x 4k (15 µm) with buried contacts
  2nd generation low noise amplifiers
    1 x 1 µm2 buried contact size
  Large format Skipper (4126 x 886)
Internal LBNL R&D funding (FY 2014)
?

## Slide 5: Outline
Major R&D areas
  Read Noise
  Readout Speed
  Quantum Efficiency

## Slide 6: Noise improvements
Development at Teledyne DALSA of buried-contact technology to reduce the floating-diffusion capacitance
4th poly layer doped p type for p-channel CCD
S. Haque et al, Proc. SPIE, 8298, 2012
Floating diffusion
47 µm / 6 µm transistor
4.3 µV/e-
3.2 e- rms at 70 kpixels/sec (-140C)
20 µm / 6 µm transistor
9.3 µV/e-
1.70 e- rms
2 x 2 µm2 buried contact

## Slide 7: Noise improvements (cont’)
Buried contact noise results for 2 x 2 µm2 buried contact
Unpublished results

## Slide 8: Noise improvements (cont’)
In progress – buried contact amplifiers on 16 channel CCDs (10.5µm) and 1 x 1 µm2 contact (mix and match lithography)

## Slide 9: Outline
Major R&D areas
  Read Noise
  Readout Speed
    Increase # amplifiers/CCD
    1st prototypes 6 and 12 channels at 512 column pitch
    Latest versions 16 channels at 512 column pitch
4k x 4k and 4k x 2k (10.5um) CCDs

## Slide 10: Readout speed improvements
Scalable CCD with amplifiers every 512 columns
  11 row taper in vertical register (10.5µm pixels)
Vertical
Serial
10.2 µm pitch
C.J. Bebek et al, Proc. SPIE, 8453, 845305-1, 2012

## Slide 11: 16 channel CCD images – 4k x 4k (10.5µm)
U band filter 500 nm narrowband filter
Images taken 4 channels at a time
200 µm thick CCD

## Slide 12: 16 channel CCD images – 4k x 4k (10.5µm)
1 µm narrowband filter
Read noise (27 channels from 4 different CCDs)
200 µm thick CCD

## Slide 13: Outline
Major R&D areas
  Read Noise
  Readout Speed
  Quantum Efficiency
    Efforts to reduce backside n+ layer thickness
    Improved anti-reflection coating materials

## Slide 14: Improving blue quantum efficiency
Good blue response requires very thin dead layers on the back surface of the CCD and appropriate anti-reflection coatings

## Slide 15: Improving blue quantum efficiency
Electric Field
y
Depletion edge
Depleted
CCD cross section
Not to scale
Back side n+ contact technology is in-situ doped polysilicon (ISDP)
  Terminates the electric field in the fully depleted substrate
  As thin as possible for blue response
  Standard for DECam was 25 nm, exploring thinner layers (15, 10, 5 nm)

## Slide 16: TEM image – 25 nm ISDP
ISDP
Low-pressure chemical vapor deposition of PH3/SiH4 at 650C
TEM image – nominal 25 nm ISDP film on silicon
(Evans Analytical Group)
PECVD SiO2
Silicon substrate

## Slide 17: TEM images – 15 and 10 nm ISDP
CCDs with good performance have been fabricated with 15 and 10 nm thick ISDP layers
~ 15 nm
~ 10 nm

## Slide 18
9.3 ± 0.25
10.5 ± 0.27
12.5 ± 0.40
11.1 ± 0.44
11.0 ± 0.35
Average thickness measurements in nm
5 process runs (150 mm wafers)
10.9 ± 1.1 nm
350nm flat field
(QE measurement)
10nm ISDP
55nm ITO
80nm SiO2
½ 4k x 4k (10.5µm)
10 nm ISDP results

## Slide 19
9.3 ± 0.25
10.5 ± 0.27
12.5 ± 0.40
11.1 ± 0.44
11.0 ± 0.35
500nm flat field
(QE measurement)
10nm ISDP
55nm ITO
80nm SiO2
½ 4k x 4k (10.5µm)
10 nm ISDP results
Average thickness measurements in nm
5 process runs (150 mm wafers)
10.9 ± 1.1 nm

## Slide 20
9.3 ± 0.25
10.5 ± 0.27
12.5 ± 0.40
11.1 ± 0.44
11.0 ± 0.35
1000nm flat field
(QE measurement)
10nm ISDP
55nm ITO
80nm SiO2
½ 4k x 4k (10.5µm)
10 nm ISDP results
Average thickness measurements in nm
5 process runs (150 mm wafers)
10.9 ± 1.1 nm

## Slide 21: Outline
Major R&D areas
  Read Noise
  Readout Speed
  Quantum Efficiency
    Efforts to reduce backside n+ layer thickness
    Improved anti-reflection coating materials

## Slide 22: Quantum efficiency – antireflection coatings
QE improvements / AR coatings
ITO index drops in the red and ITO absorbs in the blue and red
  Desire high index material with little or no absorption (rules out TiO2)
  Investigate ZrO2
  Initial work done with J. Slack (LBNL energy efficient windows group)
LBNL standard: 55/80 nm ITO/SiO2

## Slide 23: Preliminary QE – ITO/ZrO2/SiO2
Experimental data (symbols)
1-Reflectivity
  Calibration check
Theoretical model
D.E. Groom et al, “Quantum efficiency of a back-illuminated CCD imager – an optical approach,” Proc. SPIE, 3649, 80-90, 1999.
Treats silicon substrate as a thin film with QE = Absorption in silicon substrate
Models absorption in the ISDP layer (dominant loss in blue) using the SOPRA Sipoly10 n,k values (10% amorphous silicon)

## Slide 24: Preliminary QE – 10 nm ISDP with ZrO2/SiO2
UV enhanced AR coating v2
  30 nm ZrO2
  25 nm SiO2
  10 nm ISDP

## Slide 25: Quantum efficiency – standard ISDP/AR
  Standard AR coating
  55 nm ITO
  80 nm SiO2
  25 nm ISDP
200 µm thick, Vsub = 50V
Δ(1-R, QE) at long wavelengths due to absorption in the ITO

## Slide 26: Quantum efficiency – UV vs standard
UV versus standard coating
  Standard coating (25 nm ISDP)
  55 nm ITO
  80 nm SiO2
  UV coating (10 nm ISDP)
  30 nm ZrO2
  25 nm SiO2
  200 µm thick, Vsub = 50V

## Slide 27: Future efforts – broadband coatings
Calculated broadband coating QE compared to standard coating with 25 nm ISDP
  Broadband AR coating
  53 nm ZrO2
  87 nm SiO2
10 nm ISDP assumed for broadband coating
Higher red response expected due to larger index at red wavelengths (ZrO2 vs ITO)

## Slide 28: Summary – Future projects
DESI – Dark Energy Spectroscopic Instrument
  30 spectrographs (4k x 4k, 15µm pixel)
    CCD area comparable to DECam
  To be installed on Mayall Telescope (Tucson, Az) NOAO)

## Slide 29
Thank you for your attention