## Slide 1: UA Imaging Technology Laboratory
Michael Lesser
University of Arizona
Steward Observatory
UA Imaging Technology Laboratory
Production of Back Illuminated CCD and CMOS Sensors for Scientific and Industrial Imaging

## Slide 2: Outline
Recent back illuminated detector trends for scientific and industrial imaging
Back illuminated detectors overview
Novel backside detectors
Detector processing at the UAITL
Custom detector packaging
Future directions  scientific CMOS imagers

## Slide 3: Visible/UV Detector Developments
Bigger and bigger devices – 10kx10k devices
  Current limits are 150 mm wafers for CCDs, 200 mm wafers for CMOS
Extended spectral response
  UV (193 nm), X-ray, direct electron bombardment
  800 – 1000 nm QE > 80%, reduced fringing
Orthogonal Transfer Arrays (OTA)
  Split large format devices into cells
  Utilize cells independently (guiding, imaging)
  Correct for atmospheric “seeing” on-chip with OT pixels

## Slide 4: Visible/UV Detector Developments
Highly parallel outputs
  8, 16, 32, 128, 256 amplifiers
  3+ GB/sec data output per detector
Extremely tight mechanical specifications
  5 m peak-valley flatness
  -120 C operation
Large Mosaics
  Up to hundreds of devices per focal plane
CMOS imagers
  On-chip logic, low power, radiation hardened
  More manufacturing options than CCDs

## Slide 5: CCD Imaging
2x2 mosaic of 4kx4k CCDs

## Slide 6: CCD Spectroscopy
long exposures, requires very low dark current and very low noise

## Slide 7: Back Illuminated Detectors
Illuminate silicon from backside of detector rather than through frontside electronic structures
CCD cross section
back illuminated
front illuminated

## Slide 8: Back Illuminated Detectors
Why fabricate backside (expensive) devices?
  Increase quantum efficiency (QE)
    no frontside absorption/reflection
    reflection limited response is possible with appropriate backside processing
    may apply a variety of antireflection coatings for application specific optimization
  Broad spectral response
    silicon detectors are capable of excellent response from X-ray through near-IR
  Commercial backside processing
    Reduce pixel aspect ratio for very small (~1 m) pixels

## Slide 9: Ideal QE - 10 m Thick Silicon
no AR coatings

## Slide 10: Ideal QE - 50 m Thick Silicon
no AR coatings
interference fringing

## Slide 11: Ideal QE - 10, 20, 50, 100, 300 m Silicon
no AR coatings
fringing reduced for clarity
10 m
300 m

## Slide 12: Typical Visible QE

## Slide 13: Novel BI CCD Examples
STA1920A 4kx4k 16 output CCD
  ~ 100 m thick detector for LSST project (STA is Semiconductor Technology Associates, Inc.)
Transparent and conductive backside contact applied to backside for full depletion
Backside bias from guard rings around die (STA design)
Coatings optimized for near IR
prototype detector
LSST focal plane concept 3.2 Gpixels, ~200 CCDs
New LSST version of package

## Slide 14: LSST Prototype CCD
93 um thick

## Slide 15: Maintaining Good Resolution
Modulation Transfer Function is strongly influenced by charge spreading in undepleted silicon
Depletion  …silicon doping…
Must use proper Si for imager fabrication
  standard epitaxial silicon is < 100 -cm, 3 – 20 µm thick
  preferred epi for backside imagers is 100 – 5,000 -cm, up to 100 µm thick
  fully depleted devices use 5k – 10k -cm, 100 - 300 µm thick silicon

## Slide 16: Depletion – MTF
-50 V backside bias
no backside bias
Fe-55 X-ray events  point sources
LSST prototype device

## Slide 17: STA1600A 10kx10k CCD
1 die per 150 mm wafer
9 µm pixels
16 high speed outputs
~1 fps readout possible
Largest semiconductor device when first fabricated
Designed and sold by Semiconductor Technology Associates, Inc.

## Slide 18: STA1600 10kx10k CCD
<15 µm peak-valley flatness
silicon substrate
Invar package
4 cable connectors
typical operating temp. -120 C

## Slide 19: WIYN One Degree Imager
64 Orthogonal Transfer CCD focal plane to be installed on Kitt Peak next year
~ 1 Gpixel camera
SiC focal plate
ITL fully buttable package
http://www.noao.edu/wiyn/ODI/

## Slide 20: Orthogonal Transfer Arrays
Partition a conventional large-area CCD imager into an array of independently addressable cells
OT pixel
Independently
addressable cell
OTA:
8x8 Array of Cells
reduce bleed effect
OT CCDs developed at MIT/LL

## Slide 21: OTA CCD for WIYN ODI
Prototype backside device
frontside showing 64 cells
Final buttable backside device

## Slide 22: WIYN ODI – STA2200A Backside
grid projection
Fe55
image
logic glow

## Slide 23: OTAs in Action

## Slide 24: UV Semiconductor Inspection
UV laser illumination required for imaging submicron line widths
  Back illumination required for spectra response
Typical laser wavelengths
  193.5 nm, 198.5 nm, 257 nm, and 266 nm
Long-term stability difficult
  Extended UV irradiation degrades oxide and possibly backside charging mechanism

## Slide 25: BI CCDs: UV Laser imaging
UV optimized camera for industrial imaging

## Slide 26: Typical CCD Process Flow at ITL
Receive wafers from foundries
DC wafer probe (for shorts)
Image devices @ -60 C
Identify good die
Backside grind (vendor)
Gold stud bump application
Dice
Hybridize to silicon or ceramic
Epoxy underfill
Acid protection
Selective acid etch
Epitaxial acid etch
Oxidize back surface
Apply thin film coatings
Package
Characterize
Assemble focal plane

## Slide 27: Wafer Probing Detectors
OTA CCD @ -60 C
ITL Cold Prober
Which devices are good enough to go through the effort and expense of backside processing?

## Slide 28: Wafer Probing
UA “Foundry Run”
2 4kx4k CCDs
4 2688x512 CCDs
4 1200x800 CCDs
512x1024 FT guiders
128x128 AO devices
“FBI” test devices
wafer level characterization can be complex and time consuming

## Slide 29: Wafer Probing
Data from 100+ lots show yield is mainly determined on a lot to lot basis
  yield does NOT scale well with device size
Average DC yields for ‘good’ lots is > 50% (20 M criterion)
‘Bad lots’ have global issues, not just low yield
  fabrication/process problems (etching, alignments)
  silicon issues (traps, CTE, dark current)
  design problems
Very, very seldom do we see a low yield ‘good’ lot
  use multiple lots to work out issues

## Slide 30: Hybridization
bond CCD to silicon or ceramic substrate/pinned package
indium bumps mated to gold stud bumps
sizes from small 5 mm die to 250 mm focal plane
heat and pressure bonding
NASA hybridization bonder
Automated wafer stud bumper
Fiducials useful on detector and substrate

## Slide 31
Hybridization
Infrared aligner for silicon substrates
Split field aligner for ceramic substrates
All use heat, pressure, and/or ultrasonics
Various flip chip bonders used to align and bond detector and substrate

## Slide 32: Hybridization to Silicon
Silicon substrate used for majority of projects
Substrate wafer is indium bumped by electroplating
Typically hybridize a 250 µm thick detector (CCD or CMOS) to a 1400 µm thick silicon substrate
  exact thermal expansion match
  flatness spec on Si substrate is < 5 µm over 150 mm
Individual (diced) substrate die are typically flat to ~2 µm

## Slide 33: Hybridization to Ceramic
Aluminum nitride (AlN) replaces silicon as substrate material
  1-2 mm thick
Multilayer metals, vias, polished surfaces
Traces metallized and indium bumps applied
Fabricated for die or wafer level
Standard backside processing follows
Mechanical/cooling frame and connectors attached to underside
Allows combination of hybridization and packaging

## Slide 34: Hybridization Bumps
Bumps placed on wire bond pads, not in imaging area (pixels)
Regions around bumps (welts) may affect imaging, depending on geometry
Experimentally bumps have been placed under pixels for enhanced fill factor
~ 3 microns tall

## Slide 35: Epoxy Underfill
Epoxy underfill used to mechanically bond CCD and substrate after bump bonding
Heat used for viscosity control
Chip Flatteners hold device surface shape during epoxy cure
underfill stations

## Slide 36: Epoxy Underfill Ripples
We sometimes see ‘ripples’ in underfill material associated with edges of device and layout of bumps
  stress related
  ~5 m variations
  can cause issues with fiber optic bonding

## Slide 37: Silicon Etching
1:3:8 HF:HNO3:CH3COOH acid solution used to etch p+ substrate to epitaxial interface
Etch selectivity critical to achieve uniform final device thickness
Typical doping levels
  p+ = 1018 cm-3, p = 1015 cm-3
  10 – 10,000 -cm
Etch time ~2 hours

## Slide 38: Epitaxial Acid Etch
Second etch of epitaxial material to clear all p+ residual
Tailor device thickness for MTF optimization
Excessive etching decreases yield and increases cosmetic problems
Removes surface stains generated during selective etch
KMnO4 based acid solution

## Slide 39: Bulk Silicon Etching
Bulk (non-epitaxial) high resistivity silicon is used for some detectors
Improved MTF with thick devices (100-300 m)
  5k – 10k -cm silicon is typical
No epitaxial “etch stop” so 1:3:8 acid mixture does not work
Timed etch used with thickness measurements
  Hf:HNO3 mixtures
FTIR microscope for thickness measurements

## Slide 40: Acid Protection
Die/wafer edges and support substrate must be protected from etching
Wax is used as an acid resist as other materials do not survive chemistry
manual waxing
automated wax jetter
waxed stencils

## Slide 41: Custom Backside Processing
Non-thinned frame store regions for improved high speed clocking
10k CCD no shutter for Antarctica
custom space applications
thick region
thin region

## Slide 42: Backside QE Enhancement Physics
Several techniques are used to produce high QE with backside devices
Surface Charging techniques
  Chemisorption Charging (ITL)
  Flash gates (high work function materials) and UV flooding (Janesick/JPL)
Internal Charging techniques
  Implant and anneal (most common commercially)
  Delta Doping (MBE) (JPL)

## Slide 43
Backside Illumination Potentials
h
SiO2
p-Si
frontside
gate
e-
e-
n-buried
channel
backside
well
native positive charge

## Slide 44
h
SiO2
p-Si
frontside
gate
e-
e-
n-buried
channel
backside
well
-
-
-
-
-
-
native positive charge
desired negative charge
Surface Charging

## Slide 45
Internal Charging – most common
h
SiO2
p-Si
frontside
gate
e-
e-
n-buried
channel
backside
well
-
-
-
-
-
-
native positive charge
desired implant
SiO2 not required

## Slide 46: Chemisorption Charging
ITL’s Chemisorption Coating for enhanced QE
Oxidize backside of thinned CCD to reduce interface trap density
Apply thin metal film to promote negative backside charge by Chemisorption (Ag)
Apply antireflection coating optimized for application
oxidation chamber
thin films coating chamber

## Slide 47: QE Stability Critical
QE stability should be tested for all backside processes
QE vs. time, environment, and temperature

## Slide 48: Antireflection Coatings
Optimize QE for application
Broadband applications require multiple layers
UV difficult as need high index, low absorbing materials
Some common AR materials are radioactive (avoid thorium)
Common silicon BSI AR materials
  HfO2, MgF2, SiO, SiO2, Ta2O5
Use thin films design program as indices change rapidly in blue/UV

## Slide 49: Ideal QE with AR Coatings
50 m silicon
uncoated
1 layer
HfO2
2 layer
HfO2+MgF2

## Slide 50: Measured Visible QE

## Slide 51: Detector Packaging
Commercial packages
  usually not flat (~100 µm)
  not buttable
  ~$50 (Kovar, Al2O3)
Custom ceramic, invar, molybdenum, aluminum nitride
  very flat (<5 µm peak-valley)
  more stable with temperature
  better thermal transfer
  $500 - $5,000

## Slide 52
400 nm
900 nm
traces under CCD
frontside metal areas
fringing
Detector Packaging
structures under
CCD may appear when imaging
epoxy void

## Slide 53: Ultra Flat Packaging
Static dissipating ceramic vacuum chuck holds CCD on upper stage
Polished to ~1 um on both chucks
~5 um tolerance from part to part
No adjustments in focal plane assembly
Packaging jig for SNAP, ODI, Pan-STARRS
Flattest devices ±2.5 µm @ -100 C

## Slide 54: Custom BSI Packaging
Customer required backside pinout to match an existing frontside pinout (Kodak KAF-16801E 4kx4k CCD)
Multilayer aluminum nitride packages to swap signals underneath detector
top
bottom
CCD

## Slide 55: Buttable Imager Example
top
bottom
CE5 frame
AlN
indium bumps
package for WIYN One Degree Imager 64 CCD focal plane mosaic
packaged CCD

## Slide 56: Detector Flatness
Flatness at operating temperature is critical for many scientific applications
Stress reduction in processing and packaging processes are critical to achieve < 20 um flatness
WIYN ODI SN8105
Internal stresses in wafer affect device flatness (-100 C)

## Slide 57: VIEW Summit 600 CMM
Coordinate Measuring Machine in ESD safe clean room with 18”x24” measuring area, 2-3 m accuracy
WIYN ODI SiC focal plane baseplate

## Slide 58: MicroMeasure 3D Profilometry
Optical pens (interchangeable) use white light chromatic aberration technique
300 mm XY travel
non-contact
10 nm accuracy possible
24 mm max work. dist.
referenced to optical flat

## Slide 59: CryoScanner for Low Temperature
CryoScanner on isolation frame optical pen is down looking into dewar
view through dewar window
ITL built scanning system measures flatness while detectors operate cold
+25 to -150 C

## Slide 60: Back Illuminated CMOS
Early ITL CMOS thinning was 1998
Early devices used very thin epi, difficult to back illuminate without damage and latch-up issues
Typical “CCD silicon” can be used for CMOS devices which may be back illuminated without serious issues
QE is similar to backside CCDs
backside CMOS imager

## Slide 61: BI CMOS – Sarnoff/ITL
data from Jim Janesick/Sarnoff
low noise backside CMOS
on going QE enhancements

## Slide 62: Detector Characterization

## Slide 63: QE Characterization
Calibrated photodiode at detector location
Photo feedback power supply
Monochrometer (Oriel 257)
Dual filter wheels
  order blocking filters
  quartz ND filters
Integrating sphere and baffled tube
Custom UDT photodiodes
  613 mm2, UV enhanced

## Slide 64: Optical Bench One
dedicated to uniform illumination
imaging
integrating sphere
baffled tube
light sources
dewar on cart

## Slide 65: Photodiode Calibration Change
yearly calibration performed (by manufacturer – UDT)

## Slide 66: UV QE Characterization
D2 source
3 filter wheels
UV integrating cube
photodiode

## Slide 67: UV QE

## Slide 68: Summary
Backside detector processing technologies are well established and well characterized
Many scientific applications require backside devices for enhanced QE and spectral coverage
Project often have custom, cutting edge detector requirements which lead to interesting advancements
Backside CMOS processing is developing along similar path as backside CCDs and will continue to expand as enhanced CMOS imagers are fabricated
Thank you!