## Slide 1
Integrated photonic devices for controlling quantum properties of light
Qiang Lin
University of Rochester
TexPoint fonts used in EMF.
Read the TexPoint manual before you delete this box.: AAAAAAAA

## Slide 2: Outline
Introduction
Silicon devices for controlling quantum states of light
Lithium niobate devices for quantum nonlinear photonics
Summary and outlook

## Slide 3: Introduction – integrated quantum photonics
A. Politi et al, Science 320, 646 (2008).
J. Matthews et al, Nature Photon. 3, 346 (2009).
A. Peruzzo et al, Science 329, 1500 (2010).
L. Sansoni et al, PRL 105, 200503 (2010).
A. Crespi et al, Nature Comm. 2, 566 (2011).
S. Ates et al, PRL 109, 147405 (2012).
B Metcalf et al, Nature Comm. 4, 1356 (2012).
J. B. Spring, et al, Science 339, 798 (2013).
A. Crespi, et al, Nature Photon. 7, 545 (2013).
M. Tillmann, et al, Nature Photon. 7, 540 (2013).
B. J. Matcalf et al, Nature Photon. (2014).
J. Carolan, et al, Science 349, 711 (2015).
M. Poot, et al, Opt. Express 24, 6843 (2016).

## Slide 4: Introduction – integrated quantum photonics
J. Sharping, et al, OE 25, 12388 (2006).
K. Harada, et al, JSTQE 16, 325 (2010).
C. Xiong, et al, OL 36, 3413 (2011)
M. J. Collins, et al, Nature Comm. 4, 2582 (2013).
M. J. Collins, et al, OL 37, 3393 (2012).
A. Oriex et al, PRL 110, 160502 (2013).
Silica waveguide/resonator
As2S3 waveguide
J. B. Spring, et al, OE 21, 1352 (2013).
Si waveguides/resonators
LiNbO3 waveguide/resonator
Q. Zhang, et al, OE 15, 10288 (2007).
H. Jin, et al, PRL 113, 103601 (2014).
M. Fortsch, et al, Nature Comm. 4, 1818 (2013).
F. Boitier et al, PRL 112, 183901 (2014).
C. Reimer, et al, Science 351, 1176 (2016).
AlN resonator
Silicon nitride waveguide/resonator
X. Guo, et al, arXiv:1603.037261 (2016).
InGaAs waveguide
C. Xiong, et al, Optica 2, 724 (2015).
S. Ramelow, et al, arXiv:1508.04358 (2015).
R. Horn, et al, PRL 108, 153605 (2012).
S. Krapick, et al, OE 24, 2836 (2016).

## Slide 5
Photon pairs in Si microdisk
S. Rogers, et al, ACS Photon.3, 1754 (2016).
X. Lu, et al, Optica 3, 1331 (2016).

## Slide 6
Coupling induced creation pathways

## Slide 7
Coupling induced creation pathways
Cyclic evolution of Bell states
p
p
s
i

## Slide 8
Device implementation
S. Rogers, et al, ArXiv:1809.06872 (2018).

## Slide 9
Correlation characteristics
S. Rogers, et al, ArXiv:1809.06872 (2018).
Oscillation frequency matches doublet splitting

## Slide 10
Correlation characteristics
S. Rogers, et al, ArXiv:1809.06872 (2018).
High contrast oscillations  an intrinsic time-evolving path entanglement

## Slide 11
Quenching of path entanglement
S. Rogers, et al, ArXiv:1809.06872 (2018).
Small
Medium
Large
Experiment
Theory

## Slide 12
Tuning of quantum state
S. Rogers, et al, ArXiv:1809.06872 (2018).
Cavity transmission
Intracavity relative phase
On the pump mode

## Slide 13
Tuning of quantum state
S. Rogers, et al, ArXiv:1809.06872 (2018).
Laser-cavity detuning
Intracavity relative phase

## Slide 14
Tuning of quantum state
S. Rogers, et al, ArXiv:1809.06872 (2018).
Laser-cavity detuning
Intracavity relative phase

## Slide 15: Material comparison

## Slide 16: Introduction – Lithium niobate
Lithium niobate (LiNbO3) exhibits outstanding material properties:
R. S. Weis, et al, Appl. Phys. A 37, 191 (1985).
M. M. Fejer, et al, C. R. Phys. 8, 180 (2007).
W. Wang, et al, J. Micro/Nanolith.8, 031306 (2009).
Electro-optic effect
Piezoelectric effect
Pyroelectric effect
Material | Refractive index | Bandgap (eV) | Electro-optic: rij (pm/V) | Second-order nonlinear optical: dij (pm/V) | Piezoelectric: dij (pC/N)
LiNbO3 | ~2.2 | ~4 | r33 = 30.8 | d33 = 25.2 | d33 = 16, d15 = 74
Optical communications
Photonic signal processing.
…
EO modulators
Nonlinear optics
Quantum photonics
…
Wavelength converter
Wireless communications
Sensing.
…
Surface acoustic wave filter
http://www.pmoptics.com/lithium_niobate.html
http://www.smm.co.jp/E/products/material/lithium/
http://www.pmoptics.com/catvmodulator.html
https://en.wikipedia.org/wiki/Lithium_niobate
Nonlinear optical effect
Acousto-optic effect
Photorefractive effect
Photoconductive effect.
“Silicon” of photonics

## Slide 17: Conventional approaches to define LN waveguides
M. Bazzan, et al, Appl. Phys. Rev. 2, 040603 (2015).
F. Chen, et al, Opt. Mat. 29, 1523 (2007).
Method | Induced refractive index change | Disadvantage
Titanium diffusion | ~ 0.01 | Weakly guiding; dimension imprecision
Proton exchange | ~ 0.1 | Weakly guiding; dimension imprecision
Ion implantation | ~ 0.01 | Large waveguide loss, potential optical damage
D. Yang, et al, Opt. Eng. 53, 061605 (2013).
O. Yavuzcetin, et al, Opt. Mat. 36, 372 (2013).
F. Chen, et al, Opt. Mat. 29, 1523 (2007).

## Slide 18: Lithium niobate micro/nanophotonic devices
Y. S. Ilchenko, et al, Phys. Rev. Lett. 92, 043903 (2004).
A .Guarino, et al, Nature Photon. 1, 407 (2007).
T.-J. Wang, et al, Opt. Express 20, 28119 (2012)..
C. Wang, et al, Opt. Express 22, 30924 (2014).
J. Chiles, et al, Optica 1, 350 (2014).
L. Chen, et al, Optica 1, 112 (2014).
J. Lin, et al, Sci. Rep. 5, 8072 (2015).
R. Geiss, et al, Opt. Lett. 40, 2715 (2015).
S. Li, et al, Opt. Express 23, 24212 (2015).
F. Bo, et al, Adv. Mat. 27, 8075 (2015).
J. Wang, et al, Opt. Express 23, 23072 (2015).
P. O. Weigel, et al, Sci. Rep. 6, 22301 (2016).
L. Chang, et al, Optica 3, 531 (2016).
W. C. Jiang, et al, Sci. Rep. 6, 36920 (2016).
L. Chang, et al, Opt. Lett. 42, 803 (2017).
H.-D. Nguyen, et al, Opt. Express 25, 3722 (2017).
A. Rao, et al, Appl. Phys. Lett. 110, 111109 (2017).
C. Wang, et al, Opt. Express 25, 6963 (2017).
R. Luo, et al, Opt. Lett. 42, 1281 (2017).
Machining
Direct etching
Laser writing
Hybrid waveguiding
Dispersion engineering
Periodic poling
Optical Q~(107 -108)
(not on-chip)
Optical Q~105 -106

## Slide 19: Lithium niobate photonic crystals and nanocavities
R. Geiss, et al, Appl. Phys. Lett. 97, 131109 (2010).
L. Cai, et al, Opt. Lett. 39, 2094 (2014).
H. Lu, et al, Appl. Phys. Lett. 101, 151117 (2012).
H. Lu, et al, Opt. Express 20, 20884 (2012).
S Diziain, et al, Appl. Phys. Lett. 103, 051117 (2013).
M. Roussey, et al, Appl. Phys. Lett. 87, 241101 (2005).
G. Zhou, et al, Opt. Lett. 31, 2783 (2006).
N. Courjal, et al, Appl. Phys. Lett. 96, 131103 (2010).
Photonic crystals
Photonic crystal nanocavities
Fabry-Perot cavity, optical Q ~ 100
Fabry-Perot cavity, optical Q ~ 100
L3 cavity, optical Q ~ 500
J. D. Witmer, et al, Sci. Rep. 7, 46313 (2017).
Si photonic-crystal cavity on lithium niobate,
optical Q ~ 1.2105
L. Cai, et al, J. Opt. 18, 035801 (2016).
Photonic wire cavity, optical Q ~ 156

## Slide 20
Development of lithium niobate nanophotonic devices
M. Li , et al, arXiv:1806.04755 (2018).
Y. He, et al, Opt. Express 26, 16315 (2018).
H. Liang, et al, Optica 4, 1251 (2017).
R. Luo, et al, Opt. Express 25, 24531 (2017).
W. C. Jiang, et al, Sci, Rep. 6, 36920 (2016).

## Slide 21: Introduction to the photorefractive effect
Photorefraction causes resonance to blue shift.
It is generally a slow varying process.
It is unique feature to materials such as LiNbO3.
T. Volk and M. Wohlecke, Lithium Niobate (Springer, 2008).
G. T. Harvey, et al, JQE 22, 939 (1986).
T. Fujiwara, et al, Appl. Phys. Lett. 54, 975 (1989).
K. Kitamura, et al, JAP 82, 1006 (1997).
K. Buse, et al, Science 393, 665 (1998).
O. Beyer, et al, Appl. Phys. Lett. 88, 051120 (2006).
A. A. Savchenkov, et al, Appl. Phys. Lett. 88, 241909 (2006).
S. M. Korstritski, Appl. Phys. B 95, 421 (2009).
O. Beyer, et al, APL 88, 051120 (2006).
A. A. Savchenkov, et al, APL 88, 241909 (2006).

## Slide 22: On the photorefractive effect
Photo excitation to generate free carriers
P. Günter and J.-P. Huignard, eds., Photorefractive Materials and Their Applications (Springer, 2006).
Notes: Photoexite, Free carrier, drift/diffusion, recombine, trapped by acceptor, built up space charge distribution, produce electric field, change refractive index via EO effect, blue shift optical resonance.

## Slide 23: On the photorefractive effect
P. Günter and J.-P. Huignard, eds., Photorefractive Materials and Their Applications (Springer, 2006).
Carrier drift or diffusion in space
Notes: Photoexite, Free carrier, drift/diffusion, recombine, trapped by acceptor, built up space charge distribution, produce electric field, change refractive index via EO effect, blue shift optical resonance.

## Slide 24: On the photorefractive effect
P. Günter and J.-P. Huignard, eds., Photorefractive Materials and Their Applications (Springer, 2006).
Carriers recombined and trapped by impurity defects
Notes: Photoexite, Free carrier, drift/diffusion, recombine, trapped by acceptor, built up space charge distribution, produce electric field, change refractive index via EO effect, blue shift optical resonance.

## Slide 25: On the photorefractive effect
P. Günter and J.-P. Huignard, eds., Photorefractive Materials and Their Applications (Springer, 2006).
Charge redistribution to produce electric field
Notes: Photoexite, Free carrier, drift/diffusion, recombine, trapped by acceptor, built up space charge distribution, produce electric field, change refractive index via EO effect, blue shift optical resonance.

## Slide 26: On the photorefractive effect
P. Günter and J.-P. Huignard, eds., Photorefractive Materials and Their Applications (Springer, 2006).
Space-charge electric field changes the refractive index via Electro-Optic effect
 Blue shifts cavity resonance
Notes: Photoexite, Free carrier, drift/diffusion, recombine, trapped by acceptor, built up space charge distribution, produce electric field, change refractive index via EO effect, blue shift optical resonance.

## Slide 27: Photon-level resonance tuning
M. Li, et al, submitted for publication (2018).

## Slide 28: Frequency up-conversion in LN nanoresonator
H. Jiang, et al, Appl. Phys. Lett 113, 021104 (2018).

## Slide 29: Third-harmonic generation in LN nanoresonator
M. Li , et al, arXiv:1806.04755 (2018).
Second harmonic generation
Third harmonic generation

## Slide 30: Potential for ultra-strong optical nonlinearity
Shown for a telecom wavelength. It will be increased by an order of magnitude for a near-infrared wavelength (say, ~800nm).
Cavity linewidth corresponding to optical Q of 106.
: optical frequency
V: effective mode volume
deff: second-order nonlinear parameter
n0: refractive index
Effective mode volume:

## Slide 31
Broadband parametric down-conversion
SHG and PDC in LiNbO3 devices:
R. Luo, et al, Opt. Express 25, 24531 (2017).
Observation of broadband second-harmonic generation and parametric down conversion
Frequency doubling from 1549.32nm
On-chip LiNbO3 microdisk
SHG
Broadband parametric down conversion from 774.66nm,
with bandwidth > 100 nm.

## Slide 32
Waveguide length: 2.35mm.
Theoretical efficiency: 2900% W-1cm-2, experimental recorded efficiency: 650%W-1cm-2.
4 times larger than best bulk PPLN. Comparable to most recent on-chip PPLN.
Efficient frequency doubling in LN waveguides
R. Luo, et al, arXiv:1809.06476 (2018).
Potential & ongoing effort: quantum light in PT-symmetric systems.

## Slide 33: Tunable frequency doubling
Intermodal phase matching. Wavelength tuning is realized via temperature tuning.
Tuning slope ~0.84nm/K, about one order of magnitude larger than bulk PPLN.
R. Luo, et al, Optica 5, 1006 (2018).

## Slide 34: Frequency doubling in LN microresonators
Optical Q: ~ 105.
Experimental recorded efficiency: 1500%/W, theoretical value: 25000%/W.
The best result for LN microresonators. One of the best results for nonlinear microresonators.
R. Luo, et al, arXiv:1810.01299 (2018).
Potential & ongoing effort: cavity-enhanced SPDC and quantum squeezing.

## Slide 35: Self-starting mode locking of Kerr solitons
Y. He, et al, arXiv:1812.09610 (2018).

## Slide 36: Summary and Outlook

## Slide 37: Summary and Outlook

## Slide 38: Acknowledgement
Dr. Thomas Gerrits & Dr. Sae Woo Nam at NIST
Prof. Kerry Vahala’s group at Caltech
Support:
Team member:
Thank you!
Collaborator:
Hanxiao Liang
Rui Luo
Mingxiao Li
Yang He
Wei Jiang
Lithium niobate devices
Steven Rogers
Austin Graf
Usman Javid
Daniel Mulkey
Xiyuan Lu
Silicon devices
Notes: (Read all)
Thank you.

## Slide 40
Comparison of typical nonlinear optical media
M. Sheik-Bahae, et al, IEEE JQE 27, 1296 (1991).
R. DeSalvo, et al, IEEE JQE 32, 1324 (1996).
Material | Refractive index | Kerr nonlinearity n2 ( 10-7 cm2/GW) | Second-order: dij (pm/V) | Bandgap (eV)
MgF2 | 1.38 | 1.5 (@1.06m) | NA | 11
CaF2 | 1.43 | 2.5 (@1.06m) | NA | 10
SiO2 | 1.45 | 2.6 (@1.5m) | NA | 7.8
AlN | 2.12 | 23 (@1.5 m) | d33 = 4.7 (@1.5m) | 6
Si3N4 | 1.98 | 24 (@1.5m) | NA | 5
Diamond | 2.39 | 8.2(@1.5 m) | NA | 5.5
Si | 3.48 | 450 (@1.5m) | NA | 1.12
Ge | 4.0 | 3340 (@ 3.39 um) | NA | 0.67
SiC | 2.6 | 60-80 (@1.5m) | d33 = -13  -24 (@1.06m) | 2.3-3.0
As2S3 | 2.4 | 200 (@1.5m) | NA | 2.3
As2Se3 | 2.8 | 1100 (@1.5m) | NA | 1.77
ZnS | 2.40 | 168 (@1.06m) | d14 = 12 (@1.06m) | 3.54
ZnSe | 2.48 | 376 (@1.06m) | d14 = 43 (@1.06m) | 2.58
ZnTe | 2.79 | 2500 (@1.06m) | d14 = 119 (@1.06m) | 2.26
BBO | 1.6 | 5.8 (@1.06m) | d22 = 2.3 (@1.06m) | 6.2
KTP | 1.78 | 61 (@1.06m) | d33 = 14.6 (@1.06m) | 3.54
LiNbO3 | 2.2 | 18 (@1.06m) | d33 = 25.2 (@1.06m) | 3.9
GaN | 2.3 | 53 (@1.23m) | d33 = -3.8 (@1.06m) | 3.44
GaP | 3.1 | 600 (@1.04m) | d36 = 36.8 (@1.31m) | 2.2
GaAs | 3.4 | 1590 (@1.5m) | d14 = 105 (@1.5m) | 1.43
Data are from literature.

## Slide 41: Photorefractive damage in LN crystal
TexPoint fonts used in EMF.
Read the TexPoint manual before you delete this box.: AAAAAAA
D. Zheng, et al, Sci. Rep. 6, 20308 (2016).
M. Carrascosa, et al, OE 16, 115 (2008).
One major challenge to the application of lithium niobate, particular on nonlinear photonics.
Conventional mitigation approaches are to dope lithium niobate to increase damage threshold.

## Slide 42: Quenching of photorefraction
Strong saturation observed for photorefraction.
Intriguing quenching of photorefraction.
A. A. Savchenkov, et al, APL 88, 241909 (2006).
The whole process is reversible.
H. Liang, et al, Optica 4, 1251 (2017).

## Slide 43: Potential for nonlinear photonic applications
Quenching of photorefraction may find an elegant solution to the optical damage issue of LN crystal.
LN nanophotonic devices might be of great potential for nonlinear phootonic applications.
Time response of photorefraction in LN photonic crystal nanoresonator?
Photorefraction for signal processing?
M. Carrascosa, et al, OE 16, 115 (2008).

## Slide 44: Single-photon nonlinearity - Current state of the art
Atom systems require high vacuum and optical trap.
Quantum dot systems require cryogenic temperature.
Superconducting circuits require cryogenic temperature and operate at microwave frequencies.
H. J. Kimble, et al, Nature 436, 87 (2005).
K. Semba, et al, Nature Phys. 13, 44 (2017).
A. Rauschenbeutel, et al, PRL 104, 203603 (2010).
Single atom and atom cloud inside a cavity
Single quantum dot inside a cavity
M. D. Lukin, et al, Nature 508, 241 (2014).
A. Immamoglu, et al, Nature 445, 896 (2007)
Superconducting circuits.
V. Vuletic, et al, Nature 448, 57 (2013).
Challenges:

## Slide 45: Outlook
A Scalable Integrated Quantum Photonic Interconnect

## Slide 46
Compared to state-of-the-art broadband PDC
M. B. Nashr, et al, Phys. Rev. Lett. 100, 183601 (2008).

## Slide 47: Wavelength conversion in SiC devices
Conversion efficiency ~0.2/mW2

## Slide 48: Optomechanics of LN microresonators
W. C. Jiang, et al, Sci, Rep. 6, 36920 (2016).

## Slide 49: Optomechanics of LN photonic crystal nanoresonators
H. Liang, et al, Optica 4, 1251 (2017).

## Slide 50: Potential for electro-opto-mechanical hybrid coupling
K. Srinivasan, et al, Nature Photon. 10, 346 (2016).
A. N. Cleland, et al, Nature Phys. 9, 712 (2013).
GaAs
AlN
Potential for strong electo-opto-mechanical coupling.
Microwave to optical photon conversion.
Hybrid electronic – photonic signal processing mediated by high-frequency nanomechanics.
Current state of the art:

## Slide 51: Photorefractive damage in LN crystal
TexPoint fonts used in EMF.
Read the TexPoint manual before you delete this box.: AAAAAAA
D. Zheng, et al, Sci. Rep. 6, 20308 (2016).
M. Carrascosa, et al, OE 16, 115 (2008).
One major challenge to the application of lithium niobate, particular on nonlinear photonics.
Conventional mitigation approaches are to dope lithium niobate to increase damage threshold.

## Slide 52: Self-starting mode locking of Kerr solitons
Y. He, et al, arXiv:1812.09610 (2018).

## Slide 53: Frequency doubling of Kerr solitons
Y. He, et al, arXiv:1812.09610 (2018).

## Slide 54: Soliton self-frequency shift
Y. He, et al, arXiv:1812.09610 (2018).

## Slide 55: Application to integrated quantum photonics
M. Davanco, et al, APL 100, 261104 (2012).
Silicon CROW
C. Xiong, et al, OL 36, 3413 (2011)
M. J. Collins, Nature Comm. 4, 2582 (2013).
N. Matsuda, et al, OE 21, 8596 (2013).
Silicon wire waveguide
Silicon microring
Si photonic crystal
J. Silverstone, et al, Nature Photon. 8, 104 (2014).
C. Clemen, et al, OE 17, 16558 (2009).
E. Engin, et al, OE 27, 27826 (2013).
Y. Guo et al, OL 39, 2526 (2014).
D. Grassani, et al, Optica 2, 88 (2015).
J. Sharping, et al, OE 14, 12388 (2006).
H. Takesue et al, APL 91, 201108 (2007).
K. Harada, et al, JSTQE 16, 325 (2010).
p
p
s
i
p
s
i

Spontaneous four-wave mixing (FWM): Photon pair generation
Quantum interference
N. C. Harris, et al, PRX 2, 041047 (2014).
Quantum photonic circuit