## Slide 1
DISTRIBUTION A. Approved for public release: distribution unlimited. (88ABW-2016-1422)
Rochester Institute of Technology
Jeff Steidle
Greg Howland
John Serafini
Paul Thomas
Matthew van Niekerk
Mario Ciminelli
Thomas Palone
Peichuan Yin
Air Force Research Laboratory
Paul Alsing
Michael Fanto
Chris Tison
Matt Smith
Kathy-Anne Soderberg
Stefan Preble
Quantum integrated photonics
Massachusetts Institute of Technology
Dirk Englund
Tsung-Ju Lu

## Slide 2
Integrated Quantum Photonics
Motivation: Integrated photonic waveguides provide a scalable and stable platform for the implementation of quantum photon sources and circuits.
  Quantum information science requires:
    Sources of quantum bits (qubits)
    Manipulation of the qubits
    Storage of the qubits
Silicon Entangled Photon Source - CMOS Fabricated Photonic Circuit

## Slide 3
  Quantum information science requires:
    Sources of quantum bits (qubits)
    Manipulation of the qubits
    Storage of the qubits
Integrated Quantum Photonics
Quantum bit (qubit) – any two level system
  Polarization states of a photon : Horizontal or Vertical
  Energy levels in an atom : Ground or Excited
  Direction of current in a superconducting circuit: Clockwise or Counter clockwise

## Slide 4
  Quantum information science requires:
    Sources of quantum bits (qubits)
    Manipulation of the qubits
    Storage of the qubits
Integrated Quantum Photonics
Quantum bit (qubit) – any two level system
  Polarization states of a photon : Horizontal or Vertical
  Energy levels in an atom : Ground or Excited
  Direction of current in a superconducting circuit: Clockwise or Counter clockwise
Entanglement – two or more particles that interact such that they cannot be described independently.
G
E
G
E
Atom
Atom
H
V
H&V
H&V

## Slide 5
  Quantum information science requires:
    Sources of quantum bits (qubits)
    Manipulation of the qubits
    Storage of the qubits
Integrated Quantum Photonics
Superposition – every valid quantum state can be represented by the sum or two or more other distinct quantum states.
G
E
G
E
Atom
Atom
Atom 1 | Atom 2
G | G
G | E
E | G
E | E
2 particles
states
or 140 TB of space
Qubit – any two level system
  Polarization states of a photon : Horizontal or Vertical
  Energy levels in an atom : Ground or Excited
  Direction of current in a superconducting circuit: Clockwise or Counter clockwise

## Slide 6
  Quantum information science requires:
    Sources of quantum bits (qubits)
    Manipulation of the qubits
    Storage of the qubits
Integrated Quantum Photonics
Qubits are manipulated through interference.
Unit cell
Professor Dirk Englund

## Slide 7
Allows for phase and amplitude manipulation of a quantum state
  Manipulation of qubit to/from memory
Fully reconfigurable at kilohertz speeds
Interface QPP with interposer chip
  Interposer chips can be active or passive
  On-chip photon sources are possible
No feed forward currently available
Integrated Quantum Photonics

## Slide 8
  Quantum information science requires:
    Sources of quantum bits (qubits)
    Manipulation of the qubits
    Storage of the qubits
Integrated Quantum Photonics
    Trapped Ions: longest lived quantum memories
    Storage time > 15 minutes (clock states)
    Ions typically produce photons in the UV
      Ytterbium Ions – Transition at 369.5nm
      Requirement: bandgap of >3.6eV
(Trapped Ytterbium ions, AFRL)

## Slide 9
Entangling Memories
Transfer Information: Teleportation
Create ion-ion entanglement
Measure ion 2
Based on that measurement rotate the state of ion 1 before measurement to complete the teleportation protocol
369.5 nm
369.5 nm
Aluminum nitride waveguide

## Slide 10
Integrated Quantum Photonics
Motivation: Integrated photonic waveguides provide a scalable and stable platform for the implementation of quantum photon sources and circuits.
  Quantum information science requires:
    Sources of quantum bits (qubits)
    Manipulation of the qubits
    Storage of the qubits
Silicon Entangled Photon Source - CMOS Fabricated Photonic Circuit

## Slide 11
Input wave
Looking at the second term
Photon sources from Nonlinear Interactions
Polarizability
A wave of twice the frequency interacts with the fundamental waves
(second harmonic generation or spontaneous parametric down conversion)
Pump
Bi-photons

## Slide 12
ωs
ωi
Pump
Bi-photons
Nonlinear Medium
Pump 1
Pump 2
Bi-photons
=
Degenerate Four
wave mixing
Pump 1
Pump 2
Bi-photons
ωs
ωi
Photon Sources

## Slide 13
Silicon Entangled Photon Source - CMOS Fabricated Photonic Circuit
2017
Integrated Quantum Photonics

## Slide 14
Telecom wavelengths: directly interface with low loss fiber and free-space network infrastructure
Silicon photonic platform: has a strong third-order Kerr nonlinearity
UV & Telecom Photon Sources
Ultraviolet (UV) wavelengths: Directly interface to the 171Yb+ ion transition
Aluminum nitride platform: large bandgap (6.2eV) and strong second and third order nonlinearity
Yb+ ions
396nm SHG generated in AlN waveguide
Ring resonator operation in the UV (369 nm)
Frequency conversion bridges the separation between UV and Telecom

## Slide 15
Telecom Photon Sources

## Slide 16
Silicon Microring Photon Source
Correlated Photon Source – Spontaneous Four Wave Mixing (SFWM)
  χ(3) equivalent of Spontaneous Parametric Down Conversion
Silicon has a very strong third-order Kerr nonlinearity:
  n2 ~ 5E-14cm2/W, two-hundred times larger than Silica
  Strong confinement yields a large effective nonlinearity:
    ϒ~400 (Wm)-1 = ωn2/cAeff
Low Noise - Raman Scattering is narrowband and shifted ~15.6THz away from pump
Resonators enhance performance – higher brightness
Pump
Signal
Idler
Degenerate
Biphoton
Pump 1
Pump 2

## Slide 17
Demonstration of SFWM in a Ring - Device
Device Parameters:
  WG Width = 500nm
  WG Thickness = 220nm
  Ring Radius = 18.75um
  Coupler Gap = 150nm
FSR ~ 5nm
Q Factor up to 50k

## Slide 18
Pump Clean-Up
Filters
Polarization Controller
High Index SMF
Ring Resonator Circuit
Pump Rejection Filters
Superconducting Detectors
Coincidence Correlator
Arrayed
Waveguide Grating
Polarization Controllers
Pump
Laser
AWG
Power
Meter
Pump
Idler
Signal
Demonstration of SFWM – Non-Degenerate Pairs

## Slide 19
Non-Degenerate Photon Coincidences
Large CAR: >2000 with a 400ps window
  Enabled by:
    high coupling efficiency
    optimized filtering
    superconducting detectors
Larger CAR possible with narrow time windows
Pump
Signal
Idler
Narrow Bandwidth: Measured to be ~0.2 nm (25.0 GHz)
  We were limited by our measurement filter
  Resonator Bandwidth = 3.88 GHz (31.1 pm)
CAR=Coincidence to Accidental Ratio

## Slide 20
Additional Analysis
Measured Counts vs Pump Power was fit with 2nd order polynomial to determine the contribution from SFWM
Counts from SFWM can also be predicted with coincidences and system losses
Both methods are in agreement
From this and the bandwidth, the brightness was determined to be 1.32E6 pairs/s/mW2/GHz
Photon Counts
J. Steidle, M. Fanto, C. Tison, Z. Wang, S. Preble, P. Alsing, “High spectral purity silicon ring resonator photon-pair source,” Proc. SPIE 9500 (2015)

## Slide 21
Demonstration of SFWM – Degenerate Pairs
Pump Clean-up
Filters
High Index SMF
Ring Resonator Circuit
Superconducting Detectors
Coincidence Correlator
3dB
Coupler
Polarization Controllers
Power
Meter
Pump
Lasers
Polarization Controllers
3dB
Coupler
Pump Rejection Filters
Pump 1
Pump 2
Bi-photon

## Slide 22
Degenerate Photon Coincidences
CAR of ~400 with a 400ps window
CAR of up to 1000 with smaller windows
Less efficient than non-degenerate production
  Competing Non-degenerate process
Bi-Photons
Pump 1
Pump 2
Signal
Idler
Pump
Pump
Idler
Signal
J. Steidle, M. Fanto, C. Tison, Z. Wang, S. Preble, P. Alsing, “High spectral purity silicon ring resonator photon-pair source,” Proc. SPIE 9500 (2015)

## Slide 23
Spectral Selectivity
Photon generation only happens when both pumps are on their resonances - Confirmation of resonator enhanced generation of photons
Coincidences
Wavelength (nm)
Wavelength (nm)
Wavelength (nm)
Wavelength (nm)

## Slide 24
On-Chip Two Photon Interference
Device Parameters:
  WG Width = 500nm
  WG Thickness = 220nm
  Ring Radius = 18.75um
  Ring Coupler Gaps = 150nm
  Spiral Lengths ~ 1mm
  DC Gap = 150nm
  DC Length = 9um
Pump 1
Pump 2
Bi-photon
Interferometer
Photon
Source

## Slide 25
On-Chip Two Photon Interference

## Slide 26
On-Chip Two Photon Interference
Creation of a single photon:
Creation of two photons:
Creation of two-photon N00N state :
Coincidence and zero coincidence states:

## Slide 27
Two Photon Interference
“Incoherent” – Misaligned pumps
  No bi-photon generation
  Confirmation of path-entangled bi-photon quantum state
High visibility interference
Coincidences are in agreement
  Oscillates twice as fast as classical light
Physical Review Applied, August 2015

## Slide 28
Broadband Phase Matching
We achieved high visibility interference measurements for all available resonance pairs
Coincidences
Relative Phase
Notes: Amplitude variation comes from the wavelength dependence of the silicon circuit (particularly the directional coupler)

## Slide 29
Photon Loss in Microring Sources
Photon
Source

## Slide 30
Photon Loss in Microring Sources
Unfortunately, photons generated in a symmetric ring can leave through any port – an effective loss of 50%
Add
Drop
Input
Through
Add
Drop
Input
Through
Add
Drop
Input
Through
Add
Drop
Input
Through

## Slide 31
Performance Metric for Heralded Sources
Commonly used metric is heralding efficiency
  A ratio of probabilities between coincident detection and single photon detection
  Can be used for any heralded source
  Difficult to determine as it relies on absolute system losses
    IL, PDL, ,
The metric used here is coincidence efficiency
  A ratio of probabilities between coincident detection from the desired port to coincident detection from all possible ports
  Only useful for a multi-port heralded source
  Relies only on relative losses between paths in the system
    Much easier to determine

## Slide 32
Asymmetrically Coupled Microring
Add
Drop
Input
Through

## Slide 33
Asymmetrically Coupled Microring - Device
Device Parameters:
  WG Width = 500nm
  WG Thickness = 220nm
  Ring Radius = 18.75um
  Input Side Coupler Gaps = [150nm, 225nm, 300nm, 350nm]
  Output Side Coupler Gaps = 150nm
150nm
225nm
300nm
350nm

## Slide 34
Asymmetrically Coupled Microring - Setup

## Slide 35
Asymmetrically Coupled Microring - Coincidences
Device with 150nm Input Gap
Device with 350nm Input Gap
(Off-Resonance Pumping)
Fairly equal distribution of coincidences between the four possible paths
Coincidence Efficiency: 0.370
Through port coincidences primarily due to SFWM in waveguides
  Confirmed by coincidences when pump was not on resonance
10.1x the pump power required for the same power within the ring
Coincidence Efficiency: 0.967

## Slide 36
C. Tison, J. Steidle, M. Fanto, Z. Wang, N. Mogent, A. Rizzo, S. Preble, P. Alsing, “Path to increasing the coincidence efficiency of integrated resonant photon sources,” Opt. Express (2017)
Asymmetrically Coupled Microring - Results

## Slide 37
No Free Lunch?

## Slide 38
What Makes the Ideal Microring Source?
Properties of the ‘Ideal’ Microring Photon Source from Different Perspectives
From the pump photon perspective
Critically coupled
  Nothing is lost to the through port
Single-bus ring
  Pump photons trapped within the ring
High Q
  Low loss – higher power density
Over coupled – Low Q
  The photons quickly leave the ring
Single-bus ring
  All of the photons leave through the same port
From the signal/idler photon perspective
How can a single-bus ring be both critically coupled with a high Q and over coupled with a low Q?
It Can’t!
Instead, maybe a dual-bus ring can be made to act like two independent single-bus rings…
Notes: Ideally 30 minutes

## Slide 39
Interferometrically Coupled Microring Source
The use of a two point coupler makes the bus waveguide and part of the ring into a Mach-Zehnder interferometer
The easiest way understand the response of such a device is to consider the two point coupler a point coupler with the spectral dependence of a MZI

## Slide 40
Mach-Zehnder Interferometer (MZI)
Microring Resonator
Δφ
A Different Approach to Coupling

## Slide 41
Interferometric Coupling - Simulation
Device Parameters:
  WG Width = 500nm
  WG Thickness = 220nm
  Ring Radius = 15um
  Coupler Gap = 150nm
  Loss in Ring = 7dB/cm
  Path Length Difference = 47.44um

## Slide 42
Interferometric Coupling - Simulation
  WG Width = 500nm
  WG Thickness = 220nm
  Ring Radius = 15um
  Coupler Gap = 150nm
  Loss in Ring = 7dB/cm
  Input Side Path Length Difference = 47.125um
  Output Side Path Length Difference = 47.44um
Through
Add
MZI1
MZI2
Input
Drop
The addition of a second bus waveguide perfectly out of phase with the first enables the two ports of the ring to be decoupled from each other
Excess pump photons are lost in the ring
Generated photon pairs leave the ring through the drop port
Coincidence efficiency of ~100% possible with no penalty to pumping + Built-in Pump Filtering!
Device Parameters:

## Slide 43
Fabricated at SUNY Poly in Albany, NY
  Doped Si heater element
  Hermetically sealed (much better longevity)
  300mm Wafer – Lots of devices!
Si
SiO2
Si
Doped Si
Metal
Metal
Doped Si
Interferometrically Coupled Ring

## Slide 44
Exhibits behavior of asymmetrically coupled dual-bus ring resonator
  All of the resonances are supported by both sides of the device
The pump resonance is nearly critically coupled at the input side and suppressed at the output side
The signal/idler resonances are suppressed at the input side and supported at the output side
Input Side
Output Side
Non-Ideal Heater Configuration
(Equivalent to a Lossy Add-Drop Ring)
Ideal Heater Configuration
(Directional Photon Source)
Spectral Response

## Slide 45
Weakly coupled pump results in low pair generation rate.
Biased toward the drop port due to a built-in asymmetric coupling
ηcoin = 0.785
Critically coupled pump results in greatly enhanced generation rate
Negligible coincidence rates for thru and split cases
ηcoin = 0.998
Non-Ideal Heater Configuration
(Equivalent to a Lossy Add-Drop Ring)
Ideal Heater Configuration
(Directional Photon Source)
Laser Power = 5dBm
Integration Time = 300s
Laser Power = 5dBm
Integration Time = 300s
Coincidence Measurements

## Slide 46
Fine Tuning of Coincidence Efficiency
By tuning the interferometric couplers, the coincidence efficiency can be varied from less than 0.7 to (near) unity
Non-Ideal Heater Configuration
(Equivalent to a Lossy Add-Drop Ring)
Ideal Heater Configuration
(Directional Photon Source)

## Slide 47
Unentangled Photon Pairs
Vernon Z, Menotti M, Tison CC, Steidle JA, Fanto ML, Thomas PM, Preble SF, Smith AM, Alsing PM, Liscidini M, Sipe JE. Truly unentangled photon pairs without spectral filtering. Optics letters. 2017 Sep 15;42(18):3638-41.

## Slide 48
UV Photon Sources
(Qubit Storage)

## Slide 49
UV Quantum Integrated Photonic Circuits
Yb+ ions– long lifetime quantum memory, quantum repeaters
Yb+ ions
Challenge: Producing and manipulating entangled UV photons
Large refractive index (n=2.2)
Large bandgap (6eV) – Transparent above l~200nm
Large nonlinearity - n2 ~ 2 × 10-15 cm2/W
Commercially available on sapphire substrates (n=1.7)
Aluminum Nitride (AlN) Quantum Waveguide Circuits
AlN Waveguide (300x200nm)
AlN UV Photon Source (Four wave mixing):
AlN Waveguides and Ring Resonators:
Optimizing fabrication process to minimize etch roughness
Cladding based on Si-Oxy-Nitride (matched to sapphire)
Collaboration with Dirk Englund, MIT Quantum Photonics Laboratory
40 mm
5 mm
200 nm
SEM images of AlN waveguides

## Slide 50
First demonstration of fiber coupled integrated circuits at 369.5 nm
  Q > 20k
Characterization Setup
150 fs Pulsed Ti:Sapphire SHG (360-470 nm)
  Average Power up to 20 mW
  Spectrum taken from high resolution OSA
CW Tunable Ti:Sapphire SHG (367-372 nm)
  Average Power 1-10 mW
Singlemode operation in the UV (369.5 nm)
UV Integrated Photonic Circuits

## Slide 51
UV-Vis Ring Resonator Performance
Pulsed Ti:Sapphire SHG (360-470 nm)
  Pulse width ~150 fs
  Average Power up to 200 mW
Waveguide output coupled to optical fiber
Spectrum taken from high resolution OSA
  High Q’s measured 15-70K

## Slide 52
Q at 369.5 nm: ~20,000
(in literature 7K)
Propagation loss at 369.5 nm: 67-75 dB/cm
(in literature 80 dB/mm)
UV Integrated Photonic Circuits
UV (369.5 nm) Resonance

## Slide 53
Packaging

## Slide 54
AIM Photonics TAP Facility
300mm Wafer Compatibility
Chip Scale Packaging
Fiber Attach
Laser Attach
Die Attach
Wire Bonding
Wafer Dicing
High speed Electro-optic testing
Metrology
Reliability Testing
>100 Capabilities
AIM Photonics Test, Assembly and Packaging (TAP) Facility
Within the ON Semiconductor Facility
1964 Lake Ave. Rochester, NY

## Slide 55
Optical Fiber Attach
Automated Fiber Attachment
UV Curing, Laser Soldering, Micro-Welding (Nd:YAG), Filament Fusion Splicing, Laser Cleaving
Fiber Arrays (Edge Coupled)
Single Fibers
Evaluation Kits

## Slide 56
Demonstrated ultra low loss (<0.15dB) splicing between SMF-28 and ultra-high numerical aperture (UHNA) fibers.
Efficient coupling to AIM Photonic chips (with C+L Band TE/TM Edge Coupler)
  <3dB Connector-to-Connector loss
  <1dB Polarization Dependent Loss
Splicing Loss
Connector-to-Connector Loss [TE]
Connector-to-Connector Loss [TM]
Ultra-low loss splice
Efficient Coupling

## Slide 57
Thank You!
Acknowledgements