## Slide 1: Rule 07 revisited for LW and VLW
Baier N., Gravrand O., Lobre C. - CEA-LETI, MINATEC, France
Boulade O. - CEA IRFU, France
Kerlain A., Péré-Laperne N. - SOFRADIR, France
Modeling dark matter of LW MCT IRFPA
Current

## Slide 2: OUTLINE
Overall presentation of IR MCT p-on-n technology in France
Conclusion
Dark current vs temperature: results and achievements
Status of dark current from MW (5µm) to VLW (17µm) bands
Challenges to overcome in IR detection
1
2
3
4
5

## Slide 3: IR P-on-n mct at CEA-LETI & SOFRADIR A French romance
A strong link between 2 major actors of IR detection
  IR technology dev @CEA from mid 70s  1986 SOFRADIR startup
  LETI: research & transfer  SOFRADIR: improvements & FPA production
  Joint laboratory "DEFIR" to mutualize & improve our efforts
  SOFRADIR one of the 1st providers for tactical and space IRFPA
MCT p-on-n : low Jdark, low Rs  large format and HOT FPAs
Planar p-on-on photodiode
  High quality LPE epi layers
  Indium n-type extrinsic doping
  As incorporation and activation
  Process with Hg annealing
2005
1st dev
2008
1st FPA
2009
SWLW FPAs
2010
Transfert
1st product
2012
VLW FPAs
2014
SW FPAs
low dark

## Slide 4: P-on-n challenges: from HOT to LOT
Developments IR-modules: reducing Size, Weight and Power (SWaP)
  Key factor: operating at higher temperature (HOT)
  Less needs in cooling system  gain in power consumption
  No loss in perf.: NETD, dark current & operability as key parameters

## Slide 5: P-on-n challenges: from HOT to LOT
Developments IR-modules: reducing Size, Weight and Power (SWaP)
Space needs (ESA & CNES): low dark current and high cutoff wavelength
  Low flux conditions (long distance objects, transition spectroscopy, …)
  Long wavelength for earth and deep space observation
  Less constraints on operating temperature / power consumption
 Long wavelength & low dark current : 12.5µm @40K & 1400 e-/s/pix

## Slide 6: P-on-n challenges: from HOT to LOT
Developments IR-modules: reducing Size, Weight and Power (SWaP)
Space needs (ESA & CNES): low dark current and high cutoff wavelength
How to lower dark current: lower temperature?
   Tunneling current and/or depletion current
Dark current: to be limited by the lowest current
  Diffusion  dominate at high temp.
  Pure GR current  dominate at low temp.
  Depletion-type  dominate at low temp.
Reduce depletion current: increasing bandgap in space charge region  Bandgap engineering & process improvement
  Bandgap widening process
  BW not fully in SC  no reduction
  BW larger than SC  barrier ()
N type
absorbing layer
PN junction
CZT substrate
P type
cap
Ec
EF
Ev
X

## Slide 7: Dark current status in MW / LW bands at sofradir
P-on-n FPAs production @ SOFRADIR
Dark current level following Rule07
  Based on HgCdTe p-on-n technology (Teledyne) with [In]~1015 cm-3
  Verified for Teledyne, Raytheon, Sofradir
  Rule07 still reference for state-of-art IR FPA dark current
  "Diffusion limited"
SOFRADIR MW blue to LW  state of the art dark current
LWIR
MWIR blue (4.2µm)
MWIR red (5.3µm)
with
and
A. Kerlain, JEM, Vol 45-9, pp 4557-4562 (2016)
W.E. Tennant, JEM, Vol 37-9, pp 1406-1410 (2008)
W.E. Tennant, JEM, Vol 39-7, pp 1030-1035 (2010)

## Slide 8: Spectral response & QE
Addressing long wavelength with MCT: pushing the limits
100% pixel fill factor  carriers diffusion length in P-on-N
Flat QE on spectral band with mean value 50 - 85% (function of and TFPA)
Achievements @78K
NIR = 2.1 µm
SW = 2.5 µm
MW = 5.6 µm
LW = 9.3 µm
= 10 µm
= 12.3 µm
VLW = 15.1 µm
= 17.2µm
Spectral response  A/W

## Slide 9: Dark current status in LW / VLW with LPE at LETI
Dark current @78K on LPE FPAs manufactured at LETI
  From 9.3 to 17.2µm cutoff @78K: following Rule07
  No excess noise
  QE : 50 to 85% (function of and TFPA)
  Results on QVGA 30µm and VGA 15µm
QVGA - 30µm - CTIA - 100fF
QVGA - 30µm - CTIA - 6.4pF
QVGA - 25µm - DI - 0.9pF
QVGA - 30µm - CTIA - 500fF
VGA - 15µm - CTIA - 70fF
QVGA - 25µm - DI - 0.9pF
@70K
VGA - 15µm - DI - 700fF @81K

## Slide 10: Dark current status in LW / VLW with LPE at LETI
Dark current @78K on LPE FPAs manufactured at LETI
  From 9.3 to 17.2µm cutoff @78K: following Rule07
  No excess noise
  QE : 50 to 85% (function of and TFPA)
  Results on QVGA 30µm and VGA 15µm
QVGA - 30µm - CTIA - 100fF
Standard technological process

## Slide 11: Standard p-on-n reference
Standard process evaluation: reference for comparison
  1 layer with standard process (10µm cutoff @78K, 11.2µm @40K)
ROIC: VGA/2, 30µm p. pitch, snapshot, CTIA in pixel
QE: 75%
<Jdark> = 8.6e-6 A/cm²
No excess noise
QVGA - 30µm - CTIA - 500fF
78K - f/1.91 - Resp
= 10µm @78K

## Slide 12: Standard p-on-n reference: dark current status
Standard process evaluation: reference for comparison
  1 layer with standard process (10µm cutoff @78K, 11.2µm @40K)
Jdark vs Eg/kT: measured at each TFPA
  Not following Rule 07
  Best fit at high temperature with pure diffusion law
  "GR"-type depletion current
  Depletion current contribution best fit with n=4.2
Origin of this contribution
Tunnel-type current?
Transition @47K
= 10µm @78K

## Slide 13: Dark current status in LW / VLW with LPE at LETI
Dark current @78K on LPE FPAs manufactured at LETI
  From 9.3 to 17.2µm cutoff @78K: following Rule07
  No excess noise
  QE : 50 to 85% (function of and TFPA)
  Results on QVGA 30µm and VGA 15µm
QVGA - 30µm - CTIA - 500fF
VGA - 15µm - CTIA - 70fF
New bandgap widening process

## Slide 14: Bandgap widening process: results
Bandgap widening process evaluation
  2 BW variants (=11.4µm @78K, =12.7µm @40K)
 Validating BW process: lowering depletion current
QE: 80%
No excess noise
Diffusion limited @38K
QVGA - 30µm - CTIA - 500fF
78K - f/4.1 - Resp
= 11.4µm @78K
Transition @38K
50K
40K
67K
30K
25K

## Slide 15: Bandgap widening process: results
Bandgap widening process evaluation
  2 BW variants (=11.4µm @78K, =12.7µm @40K)
= 11.4µm @78K
@32K
= 12.8µm <Jdark> = 1050 e-/s
2.5e-11 A/cm²
1400 e-/s/pix
40K
Requirements (ESA)
(12.5µm @40K)
Rule07 is not diffusion
underestimate Jdark
10 lower @40K
50K
40K
67K
30K
25K

## Slide 16: Dark current: Beyond Rule07
Rule07 is a good dark current predictor @78K
But not for Jdark(T), following diffusion law
Rule07 convenient: fixed parameters
Diffusion fit:
adapted for each FPA
(7 FPAs tested)
From Rule07 @78K
50K
40K
67K
33K

## Slide 17: Are we alone in dark current universe?
Data from NEOCAM instrument @Rochester University
  Teledyne LW MCT on H1RG
C. McMurtry, Optical Engineering, Vol 52 (9), 091804-1 (2013)
Rule07 underestimate Jdark: 10 lower @40K
Low-temp revisited Rule07:
 Right slope
 Still a factor 1.8
= 10.6µm @30K
50K
40K
33K

## Slide 18: Conclusion
P-on-n MCT LPE technology @ DEFIR
Demonstration on FPAs
 LW to VLW 17.2 µm @78K
 Low dark current ≈ 1k e-/s/pix with 12.8 µm @32K
 50 - 85% QE
Rule07 works @78K in LW / VLW
  Is not a diffusion trend line
 At low temperature: underestimate Jdark
Dark current (, T)
  Diffusion trend line till 50-40K  intrinsic depletion-type current
 Diffusion Rule7FPAs: work in progress

## Slide 19
Thank you
For your
Attention