## Slide 1: Characterization of single-photon sensing and photon-number resolving CMOS image sensors
Justin P. Gallagher, Lazar Buntic, Don F. Figer
Center for Detectors, Rochester Institute of Technology, Rochester, NY

## Slide 2: Outline
Testing Equipment and Image Sensors
Detector Characterization
Astronomical Observations
Conclusions

## Slide 3: Testing Equipment AND Image Sensors

## Slide 4: Rochester Imaging Detector Lab (RIDL) Experiment Test Suite
SpectraPro-2500i
SP-2555
Spectrometer
QTH
Light Source
Filter Wheel
Slit
Integrating Sphere
Diode
Port for Detector/Dewar

## Slide 5: The Quanta Image Sensor (QIS)

## Slide 6: The QIS Concept
Eric R. Fossum (Dartmouth College), Gigajot Technology Inc.
small floating diffusion (FD) sense node
small FD capacitance increases voltage response to charge
single-electron voltage response much larger than read noise
correlated multiple sampling to further reduce noise
discrete photoelectron peaks become resolved

## Slide 7: Correlated Multiple Sampling (CMS)

## Slide 8: The QIS Pathfinder
twenty 1Mpix QIS
1024×1024 pixels
1.1 μm pixel pitch
parallel-cluster rolling shutter
optional: 1(H)×2(V) pixel charge domain binning

## Slide 9: The QIS for Cryogenic Testing (QISSAT)
near identical chip to QISPF
mounted on 224-pin ceramic chip carrier
operated by custom electronics developed by RIT
operated at 200 K – 300 K in vacuum
presented results are from one image sensor on one chip

## Slide 10: The QIS Camera Development Kit (QISCDK)
16.7 Mpix QIS (GJ01611)
4096×4096 pixels
1.1 μm pixel pitch
parallel-cluster rolling shutter
thermoelectric cooler keeps sensor at 10C
USB3.0 data rate limits camera to 14 fps

## Slide 11: QISCDK: Low Light 16.7 Mpix Images

## Slide 12: Detector Characterization

## Slide 13: Detector Characterization Table

## Slide 14: Photon-Number Resolution

## Slide 15: Conversion Gain of Sensor Array

## Slide 16: Dark Current vs Temperature

## Slide 17: Read Noise and CMS

## Slide 18: Quantum Efficiency

## Slide 19: Photon Transfer: Linearity and Full-Well Depth

## Slide 20: Persistence

## Slide 21: Characterization Summary for NASA Applications

## Slide 22: Astronomical Observations

## Slide 23: Raw and Processed Images from Observations
The Lunar Surface of Copernicus, Kepler, and the Mare Insularum
Saturn (70 ms integration)
M13 Raw Inverse-Heatmap
M67 Process False Color Image
Notes: The lunar surface photo includes Copernicus (large rightmost crater), Kepler (middle crater), and Aristarchus (top left crater on photo edge). Mare Insularum (Sea of islands) located between Copernicus and Kepler.

## Slide 24: Conclusions

## Slide 25: Summary
four single-photon sensing and photon-number resolving 1.1 μm QIS devices were tested
dark current of 0.002 e-/s at 267 K
median read noise of 0.21 e-
QE of >85% at 500nm
QE of >17% at 920nm (water vapor absorption)
aperture photometry of M13 and M67
preparing devices for radiation testing in future

## Slide 26: Thank you
Justin P. Gallagher
jpgcfd@rit.edu
Donald F. Figer
figer@cfd.rit.edu
Lazar Buntic
lb4525@rit.edu

## Slide 27: Backup Slides

## Slide 28: QISSAT: Dewar and Custom Electronics

## Slide 29: Electronic Gain

## Slide 30: Electronic Gain

## Slide 31: Read Noise Evaluated from Two Different Methods

## Slide 32: M13 aperture photometry

## Slide 33: Dark Current Slopes